## Slide 1: Design and analysis of Steel Connection Types
Prepared by: Dr. Rachel Chicchi , University of Cincinnati
with the support of the American Institute of Steel Construction
Some Slides Courtesy of Dr. James Swanson, University of Cincinnati
2. Bolts & Welds Basics
Version 1 – January 2022
Notes: This series of PowerPoint presentations covers the fundamentals of the design and analysis of steel connections. The intention of these slides was to focus on simple (shear) connections and include all aspects of connection design and detailing, including design procedures and constructability considerations. Given the volume of the content, basic fundamentals were provided which do not dig in closely to the design portion of the connections. If you would like slides related to specifics of shear connection design, you may reach out to Rachel Chicchi to obtain these additional slides.
The material can be used at the graduate or undergraduate level. Portions can also be used for construction management or architecture students.
This module is #2 – Connection Basics: Bolts & Welds
This module uses a number of code/references: AISC 360-16, RSCS 2020, AWS D1.1-2020. The version of RCSC in the 15th Edition of the Steel Manual is 2014, but RCSC updated their specification in 2020. The primary change to this was updated bolt group classifications. In order to give students the most up-to-date information, we have primarily chosen to include information from the 2020 RCSC instead of 2014. For those wishing to teach from the RCSC 2014, notes are provided in the slides to distinguish changes between the two editions.
For questions, comments, corrections, or suggestions on these presentations, please contact:
Rachel Chicchi
Civil & Architectural Engineering and Construction Management
University of Cincinnati
2850 Campus Way Drive
765 Baldwin Hall
Cincinnati, OH 45221
Email: rachel.chicchi@uc.edu
Acknowledgments:
These presentations were prepared with support from the AISC Teaching Aid Development Program. Overall coordination of this effort was provided by Kristi Sattler at AISC. The author gratefully acknowledges support provided by AISC and the coordination and oversight provided by Dr. Sattler.
The author also gratefully acknowledges contributions and review provided by the AISC review committee for this project:
Hans Herrmann – Mississippi State University
Jason McCormick – University of Michigan
Tim Mrozowski – Michigan State University
Thank you also to Dr. James Swanson at the University of Cincinnati for providing a number of slides and images for this module.

## Slide 2: Design and analysis of steel connections
1 - Introduction, Basic Principles, and Limit States
2 - Connection Basics: Bolts & Welds
3 - Constructability Considerations
Notes: This PowerPoint series is divided into 3 modules. This is the second module on connection basics: bolts and welds.
Note that there were 3 other modules previously planned. Refer to the ReadMe for information on these modules and feel free to contact the author with requests for these additional files.

## Slide 3: 2- Connection Basics: Bolts and Welds
Bolts
  Bolt grades
  Bolt connection types
  Bolt installation methods
  Bolt sizes and hole sizes
  Dimensional limitations
Welds
  Weld processes
  Weld types
  Dimensional limitations
  Weld Symbols
Notes: Focus will first be given to the basics of bolts. Then welding will be covered.

## Slide 4: Bolts – helpful resources
AISC Specification - Chapter J Design of Connections *
RCSC Specification for Structural Joints Using High- Strength Bolts*
AISC Manual Part 7 – Design Considerations for Bolts
AISC Design Guide 17: High Strength Bolts –A Primer for Structural Engineers+
* available for a free download from AISC.org or boltcouncil.org
+ available for free from AISC.org with free AISC Student Membership
Notes: The PDF versions of all AISC Design Guides are available for free download by AISC Educator and Student Members at https://www.aisc.org/publications/design-guides/design-guide-pdfs
Note: When students purchase a Steel Construction Manual through the Manual Discount Program, they are automatically enrolled as AISC Student Members.

## Slide 5: Rivets (historic fastener)
Rivets are no longer used in new design.
Notes: Design provisions for rivets were omitted from the AISC Specification beginning in 2005 and their use in new construction has become obsolete, but you may see them in existing structures.
Rivets are made from bar stock by either hot- or cold-forming the manufactured head. The head is usually of the high button-type, although flattened and counter-sunk rivets are made for applications with limited clearance. In North America, rivets are now seldom used in new work. Bolts, either ordinary (A307) or high-strength (A325 and A490), provide an equal or superior connection, and their installed cost is less than that of rivets.
AISC Design Guide 15 on rehab and retrofit provides more commentary on rivets in existing connections.
Source : Guide to Design Criteria for Bolted and Riveted Joints, G. Kulak

## Slide 6: Bolts
Notes: Bolts are the most common steel fastener used in connections today.
Source: Guide to Design Criteria for Bolted and Riveted Joints, G. Kulak

## Slide 7: Structural Bolts & Rivets
(ASTM F3125, Group A)
(ASTM F3125, Group B)
Notes: The ASTM specification for structural rivets, A502, provided three grades, 1, 2, and 3. Grade 1 is a carbon steel rivet for general structural purposes, Grade 2 is for use with higher strength steels, and Grade 3 is similar to Grade 2 but has atmospheric corrosion resistant properties. The only mechanical property specified for rivets is hardness. The stress vs. strain relationship for the different strength levels is shown in the figure. (The plot shown represents the response of a coupon taken from the parent rivet or bolt.) Since the only reason for dealing with rivet strength today is in the evaluation of an existing structure, care must be taken to ascertain the grade of the rivets in the structure. Very old structures might have rivet steel of lesser strength than that reflected by ASTM A502. (This ASTM standard, A502, was discontinued in 1999 though it has since been reaffirmed and is a current standard.)
Source: AISC Design Guide 15
Remember that rivets should not be used in new structures and are simply provided here so that you can see the difference in bolt and rivet behavior.
Also note that alpha groups will be gone in the 2022 version of the Specification.

## Slide 8: Structural Bolts
  Structural bolts are commonly high strength bolts that comply with ASTM F3125 or F3148.
  They come in multiple types:
  - Heavy hex head or button head
  - Plain ends, fixed splines or twist-off splines
  - Plain or weathering
  - Different strengths (120, 144, 150 and 200 ksi tensile)
  - Non-coated or coated

## Slide 9: Specifying bolt design
  Connection designer typically specifies bolt grade, nominal diameter, hole size, and whether threads are permitted in the shear plane.
  Bolt length determined by steel detailer/ fabricator.
  i.e.
  ¾” diameter ASTM F3125 Grade A325 N with standard hole
Nominal diameter
Bolt type and grade
Threaded condition
Hole size
Notes: The connection designer specifies the threaded condition. This is a use condition: you do not order X bolts or N bolts. The fabricator/detailer will ensure an N or X condition when detailing the connection and determining bolt length.

## Slide 10: Bolt GROUPS
  High-Strength Bolts (AISC - J3.1) – shall conform to the provisions of the Specification for Structural Joints Using High-Strength Bolts (RCSC Specification)
  Group A: High-Strength Medium Carbon Steel (Fu = 120 ksi)
  ASTM F3125 Grades A325 and F1852, and ASTM A354 Grade BC
  ASTM F3125 - Most commonly used in building construction
  Use ASTM A354 only where size or length prohibits the use of F3125
  Group B: High-Strength Heat Treated Steel (Fu = 150 ksi)
  ASTM F3125 Grades A490 and F2280, and ASTM A354 Grade BD
  Use ASTM A354 only where size or length prohibits the use of F3125
Notes: Note: Bolt group designations will be updated in the 2022 Specification to comply with 2020 RCSC.
In 2020 RCSC, ASTM F3125 are Group 120. A354 only used where size or length does not permit F3125 to be used. Group 144 and Group 150 have replaced Group B. The designation is based on tensile strength.

## Slide 11: Bolt groups
  Group C: (Fu = 200 ksi)
  ASTM F3043 (twist off) and ASTM F3111 (heavy hex)
  ASTM A307: Carbon steel (Fu = 60 ksi)
  Machine bolts, not commonly used.
  Used for secondary members
Notes: Group C are not currently available in the market, but they will be. They are remaining in the AISC Spec but do not appear in the RCSC Spec. In AISC they are now Group 200.

## Slide 12: Bolt groups
Note: Bolt group designations changed from RCSC 2014 to RCSC 2020.
Group 120 – formerly Group A ; Group 150 – formerly Group B
RCSC 2020
Notes: RCSC’s 2020 specification has changed the classifications of the bolts. These will be updated in AISC 360-22. RCSC 2014 is what is currently specified in the 15th Edition of the Steel Manual.
Group 120 was formerly Group A.
Group 150 was formerly Group B.

## Slide 13: Bolt Joint types
Bearing Type
  X – threads excluded from shear plane
  N – threads included in shear plane
shear plane
Threads Not Excluded
Threads eXcluded
Notes: One (or maybe the only difference) between structural bolts B18.2.6 and other heavy hex bolts B18.2.2 is that the thread is shorter to improve the chances of using X bolts.

## Slide 14: Bolt Joint types
Bolts primarily rely on bearing to transfer forces between the plies.
If bolts are sufficiently tightened and plies adequately prepared, friction may contribute to force transfer.
Bearing or friction type connections depend on the bolt installation method.
Notes: Preparation of plies includes blasted and or coated surfaces.

## Slide 15: Bolt Joint types
Bearing
Friction
Notes: In bearing joints, the design criteria is based upon the shear strength of the bolts and the bearing strength of the connected materials.
In friction joints, loads are also transferred through friction resulting from the clamping of the bolt. This clamping creates a normal force between the plates (aka faying surfaces) that creates friction.

## Slide 16: Bolt Joint types
Joint Type
  Snug-tightened Joint
  Pretensioned Joint
  Slip-critical Joint
Notes: Snug-tight high-strength bolts are permitted for all bearing joints except when fully tensioned (bearing or slip-critical) bolts are required per the AISC Specification and the RCSC Specification. For example, high-strength bolts must be fully tensioned for:
1. Slip-critical connections, RCSC, Section 4.3.
2. Connections where the bolts are subject to direct tension loading.
3. Column splice connections in tier structures that are 200 ft or more in height, 100 to 200 ft in height if the least horizontal dimension is less than 40% of the height, or less than 100 ft in height if the least horizontal dimension is less than 25% of the height.
4. In structures over 125 ft in height, connections of beams and girders to columns and of any other beams and girders upon which the bracing of columns is dependent.
5. In structures carrying cranes with a capacity of over five tons, roof-truss splices and connections of trusses to columns, columns splices, column bracing, knee braces, and crane supports.
6. Connections for supports of running machinery or of other live loads that produce impact or stress reversal.
7. Other connections stipulated as fully tensioned on the design plans.
Source: AISC Steel Solutions Center FAQs (https://www.aisc.org/steel-solutions-center/engineering-faqs/6.5.-bolt-installation/)
Note that slip-critical joints are the most expensive, then pretensioned. Snug-tightened is the least expensive.

## Slide 17: Bolt Joint types
Snug-Tightened Installation
Notes: The snug-tightened condition is the tightness that is attained with a few impacts of an impact wrench or the full effort of an ironworker using an ordinary spud wrench to bring the plies into firm contact.
Other tools include: spuds, other hand wrenches only for unusual conditions, electric, pneumatic, and hydraulic wrenches.
Entering and tightening clearances are also an important consideration when detailing connections. Refer to Part 7 of the Steel Construction Manual (Table 7-15 and Table 7-16) for clearance requirements.

## Slide 18: Bolt Joint types
Snug-Tightened Joints (RCSC 2020, 4.1)
Bolts are permitted to be installed snug tight when:
  Used in bearing-type connections
  Group 120 (previously Group A) bolts are used in connections subjected to tension or combined shear and tension where loosening or fatigue due to vibration or load fluctuations are not considerations
  Bolts to be tightened to a condition other than snug tight shall be clearly identified on the design drawings.
Notes: The RCSC Specification defines a snug-tightened joint as a joint in which the bolts have been installed in accordance with Section 8.1. Note that no specific level of installed tension is required to achieve this condition, which is commonly attained after a few impacts of an impact wrench or the full effort of an ironworker with an ordinary spud wrench. The plies should be in firm contact, a condition that means the plies are solidly seated against each other, but not necessarily in continuous contact. There is no upper limit to the pretension that can be present in a snug-tightened joint. Twist-off-type tension-control bolts can be used in snug-tightened joints, even if the splined ends are severed during installation.
It is a simple analogy to say that a snug-tight bolt is installed in much the same manner as the lug nut on the wheel of a car; each nut is turned to refusal and the pattern is cycled and repeated so that all fasteners are snug. Essentially, snug-tight bolts utilize the higher shear/bearing strength of high-strength bolts with installation procedures similar to those used for ASTM A307 common bolts, which are never fully tensioned.
Hence, the majority of bolted connections in buildings need only use snug-tightened bolts, i.e., the bolts are installed using the full effort of an ironworker with a spud wrench. This is the most economical way of making bolted connections in buildings because no compressed air or attendant equipment is needed, washers may not be required, and inspection is simple.
Source: AISC Steel Solution Center FAQs (https://www.aisc.org/steel-solutions-center/engineering-faqs/6.5.-bolt-installation/).
Not that the economy of these joint types comes from the lack of procedures required to achieve a specified minimum pretension and inspection.

## Slide 19: Bolt Joint types
Snug-Tightened Joints
AISC 2016: The snug-tight condition is defined in the RCSC Specification.
RCSC 2014: “The snug tightened condition is the tightness that is attained with a few impacts of an impact wrench or the full effort of an ironworker using an ordinary spud wrench to bring the plies into firm contact.”
RCSC 2020: “The joint condition in which the plies have been brought into firm contact and each bolting assembly has at least the tightness attained with either a few impacts of an impact wrench, resistance to a suitable non-impacting wrench, or the full effort of an ironworker using an ordinary spud wrench”
Notes: AISC has adopted the RSCS definition of “snug-tight”. It is admittedly a term that has been difficult to define precisely and it’s definition has evolved slightly since RCSC 2014.

## Slide 20: Bolt Joint types
Pretensioned Joint (RCSC, 4.1)
Where the bolts are required to be fully tensioned but the slip resistance is not relied upon to transfer load.
Appropriate when pretension is desired for reasons other than slip resistance.
Pretensioned joints have some additional installation costs over snug-tightened joints.
Notes: RCSC, AISC, and AASHTO require that the designer identify whether the bolts used must be pretensioned or need only be snug-tightened. The design documents must indicate the intention of the designer. In this way, the plan of the designer when the joint was proportioned will be fulfilled by those responsible for the shop fabrication, field erection, and inspection of the work.
Bridges—In the great majority of cases, it will be required that the joints not slip under the action of the repetitive load that is present in all bridges. In the terminology of the RCSC Specification, this means that the joints must be designated as slip-critical. The AASHTO Specification permits bearing-type connections only for joints on bracing members and for joints subjected to axial compression. It is likely that most bridge documents will require slip-critical joints throughout in the interest of uniformity.
Buildings—The requirements for buildings allow more latitude in the selection of bolt installation. It is not usual for a building to have moving loads, and wind and earthquake forces are not considered to result in fatigue. Consequently, the need for pretensioned and slip-critical bolts is not as frequent in buildings as it is for bridges.
Source – AISC Design Guide 17

## Slide 21: Bolt Joint types
Pretensioned Joint (RCSC 2020, 4.1)
Pretensioned joints are required in the following applications:
  Joints in which fastener pretension are required in the Specification;
  Joints that are subject to significant load reversal;
  Joints that are subject to fatigue load with no reversal of the loading direction;
  Joints with Group 120 bolting assemblies that are subject to tensile fatigue;
  Joints with Group 144 or Group 150 bolting assemblies that are subject to tension or combined shear and tension, with or without fatigue.
Notes: For buildings, only in certain cases is it required that the bolts be installed so as to attain a specified minimum pretension. These are enumerated in the RCSC Specification and they include (a) joints that are subject to significant load reversal, (b) joints subject to fatigue, (c) joints that are subject to tensile fatigue (A325 and F1852 bolts), and (d) joints that use A490 bolts subject to tension or combined tension and shear, with or without fatigue.
The bolt installation costs and inspection for joints requiring pretensioned bolts will be higher than if the bolts need only be snug-tightened. Slip critical joints are more expensive than pre-tensioned joints.
Source – AISC Design Guide 17
A brief history of fasteners:
Rivets were all tightened. Then there were high strength bolts (HSBs) all tightened. Then bolts subject to shear were permitted to be snug. Then, in the 90s some testing was done resulting in permitting some Group 150 bolts subjected to tension or combined to be snug. Thus, Group 144&150 subject to tension have to be pretensioned.

## Slide 22: Bolt Joint types
Minimum Bolt Pretension for Pretensioned or Slip-Critical Joints
AISC 360-16
In 15th Edition of Steel Manual
Includes former group designations
Notes: All high-strength bolts specified on the design drawings to be used in pretensioned or slip-critical joints shall be tightened to a bolt tension not less than that given in Table J3.1.
Torque is an invalid measure for fully tensioned installation, unless it is calibrated. In 1951, the first RCSC Specification incorporated a table of standard torque values for the installation of fully tensioned high-strength bolts. However, depending upon the condition of the threads, it was demonstrated that the resulting installed tension varied by as much as plus or minus 40 percent. It is now known that clean, well lubricated threads result in tensions that are higher than required (and probably a few broken bolts), whereas, rusted, dirty, or poorly lubricated threads result in tensions that are below the minimum required. Therefore, recognition of these standard torque values has long been withdrawn.
Accepted procedures for fully tensioning high-strength bolts can be found in the RCSC Specification Section 8.2. If torque is to be used as in the calibrated wrench method as described in the RCSC Specification Section 8.2.2, it must be calibrated on a daily basis for the lot, diameter, and condition of bolts being installed.
Source: AISC Solution Center FAQs (https://www.aisc.org/steel-solutions-center/engineering-faqs/methods-for-fully-tensioned-installation/)

## Slide 23: Bolt Joint types
Minimum Bolt Pretension for Pretensioned or Slip-Critical Joints
RCSC 2020
Will be in 16th Edition of Steel Manual
Includes new group designations
Notes: RCSC 2020 will be referenced in the 16th Edition of the Steel Construction Manual.

## Slide 24: Bolt Joint types
Slip-Critical Joint (RCSC 4.3)
RCSC: A joint that transmits shear loads in which the bolts have been installed to provide a pretension in the installed bolt (clamping force on the faying surfaces), and with faying surfaces that have been prepared to provide a calculable resistance against slip.
AISC: Bolted connection designed to resist movement by friction on the faying surface of the connection under the clamping force of the bolts.
Slip-critical joints are appreciably more expensive because of the associated costs of faying surface preparation and installation and inspection requirements.
Notes: Slip-critical bolts are not always needed at moment and brace connections, and bearing bolts might be acceptable in standard holes. The RCSC (Research Council on Structural Connections) Specification, Section 4.3 gives criteria for slip-critical joints, which are more costly than bearing joints due to additional installation, inspection and faying-surface preparation. Also, more or larger bolts are needed for reduced bolt strength. In certain conditions, fabricators/erectors might prefer slip-critical bolts for oversized holes and greater erection tolerance. If slip-critical joints and bolts are needed, the steel detailer must indicate them on the erection and shop drawings. The detailer should indicate masking requirements in the bolt-hole area to keep the faying surface free of coatings from inadvertent overspray of unqualified paint.
This type of connection is used mainly in bridges, where fatigue is a consideration. In buildings, wind is not considered to be a fatigue phenomena. However, if oversize holes or slotted holes that run parallel to the direction of the member forces are used, slip-critical connections are required in buildings. The RCSC Specification does stipulate that slip-critical connections be used when "slip at the faying surfaces would be detrimental to the performance of the structure." This is generally interpreted to include the joints in lateral bracing systems. It is important to note also that connections that must resist seismic forces need to receive special attention.
If slip-critical connections are used unnecessarily in buildings, higher installation and inspection costs will result.
Source: AISC Design Guide 17

## Slide 25: Bolt Joint types
Notes: Table Source: https://www.aisc.org/globalassets/modern-steel/archives/2016/01/steelwise.pdf
Slip in bolted connections is not a structural concern for the majority of connections in steel building structures. The RCSC Specification Commentary Section 4.1 states that “The maximum amount of slip that can occur in a joint is, theoretically, equal to twice the hole clearance. In practical terms, it is observed in laboratory and field experience to be much less; usually about one-half the hole clearance. Acceptable inaccuracies in the location of holes within a pattern of bolts usually cause one or more bolts to be in bearing in the initial, unloaded condition. Furthermore, even with perfectly positioned holes, the usual method of erection causes the weight of the connected elements to put some of the bolts into direct bearing at the time the member is supported on loose bolts and the lifting crane is unhooked. Additional loading in the same direction would not cause additional joint slip of any significance.” In some cases, slip resistance is required. The AISC and RCSC specifications list cases where connections must be designated by the structural engineer of record as slip-critical:
1. Joints that are subject to fatigue load with reversal of the loading direction
2. Joints that utilize oversized holes
3. Joints that utilize slotted holes, except those with applied load approximately normal (within 80° to 100°) to the direction of the long dimension of the slot
4. Joints in which slip at the faying surfaces would be detrimental to the performance of the structure
5. The extended portion of bolted, partial-length cover plates, as required in AISC Specification Section F13.3
6. Bolted connections with undeveloped fills, as required in Section 573 J5.2.(d)
One special case also exists. A nominal amount of slip resistance is required at the end connections of bolted built-up compression members so that the individual component will act as a unit in column buckling. As specified in the 2005 AISC Specification Section E6.2, “The end connection shall be welded or pre-tensioned bolted with Class A or B faying surface.”
Source: AISC Steel Solutions FAQs (https://www.aisc.org/steel-solutions-center/engineering-faqs/6.5.-bolt-installation/#9569)

## Slide 26: Bolt joint types
RCSC 2020
Notes: Table from RCSC, 2020 – summarizes the applications and requirements for joint types: snug-tight, pretensioned, slip-critical
The table from RCSC 2014 is similar.

## Slide 27: Methods of bolt installation
AISC: Installation shall comply with the RCSC Specification
RCSC (2020): One of the pretensioning methods in Sections 8.2.1 through 8.2.5 shall be used:.
Section 8.2.1: Turn-of-Nut Pretensioning
Section 8.2.2: Calibrated Wrench Pretensioning
Section 8.2.3: Twist-Off Tension-Control Bolt Pretensioning
Section 8.2.4: Direct-Tension-Indicator Pretensioning
Section 8.2.5: Combined Method Pretensioning (new in RCSC 2020)
Notes: Provisions in the RCSC Specification (2014) Section 8.2 include four methods for the pre-tensioning of high-strength bolts. The use of these procedures is governed by the provisions listed below: turn-of-nut pre-tensioning, calibrated wrench pre-tensioning, twist-off-type tension-control bolt pre-tensioning, and direct tension indicator pre-tensioning. RCSC also allows the use of alternative-design fasteners and alternative washer-type indicating devices. When used properly, each method can produce properly tensioned high-strength bolts. (In RCSC 2020, the combined method was added. It can be used on plain end bolts but was added to install fixed spline end bolts.)
Regardless of the method used, pre-installation verification must be performed, the snug-tight condition must be achieved prior to pre-tensioning, washers must be positioned as required in Section 6.2, and installation should commence at the tightest part of the joint and progress toward the free edges. Several cycles may be needed to achieve a snug tight condition.
A Skidmore-Wilhelm Bolt Tension Calibrator, manufactured by the Skidmore-Wilhelm Manufacturing Company (www.skidmore-wilhelm.com) can be used for measuring tension in a bolt for a variety of installation methods. When a sample bolt is installed in the “Skidmore,” the tension is measured on a dial gauge. Thus, the appropriate torque for use in the calibrated wrench installation method may be determined, or the proper tension resulting from the turn-of-nut, alternative design bolt, or direct tension indicator methods may be verified. It is not intended that the use of other similar devices be excluded by this discussion.
Alternative designs are also permitted.
Source: AISC Steel Solutions Center FAQs (https://www.aisc.org/steel-solutions-center/engineering-faqs/methods-for-fully-tensioned-installation/#9575)

## Slide 28: Methods of bolt installation
Turn-of-nut Pretensioning involves several steps:
The bolt is snug-tightened
Match marks may be placed on each nut, bolt, and steel surface in a straight line (recommended, not required)
The part not turned by the wrench is prevented from turning
The bolt is tightened with a prescribed rotation past the snug-tight condition
Turning the nut imposes a lengthening of the fastener, i.e. an initial strain, which correlates to an initial stress.

## Slide 29: Methods of bolt installation
Tightened
Not Tightened
Turn-of-nut Pretensioning
Notes: The fact that a nut and hex head has 6 sides makes it easier to determine whether the proper turn has been applied as it is typically specified in thirds or sixths.
Photo Courtesy of Dr. James Swanson, UC

## Slide 30: Methods of bolt installation
RCSC/AISC 348-14
Notes: Application of the installation torque need not produce a relative rotation between the bolt and nut that is greater than the rotation specified in Table 8.2
The minus 30 deg tolerance was removed in RCSC 2020.

## Slide 31: Methods of bolt installation
Calibrated Wrench Pretensioning
Calibrated Wrench pretensioning uses a wrench that is capable of measuring the applied torque.
There is a repeatable relationship between the torque applied to the nut and the tension induced in the bolt.
RCSC-20 now limits the use of this method because of the scatter in the torque / tension relationship.
Notes: A sample of bolts to be used in the connections are tested to determine the torque level required to achieve the correct tension.
There is a relationship but it has significant scatter so RCSC requires extra measures to reduce the variables. Friction is in the threads and under the bearing surface of the turned element. A change in RCSC-20 adds severe limits to where this method can be used. Turn only the nut means you cannot use where driving clearance is not available at the nut.

## Slide 32: Methods of bolt installation
Calibrated Wrench Pretensioning
A Skidmore-Wilhelm tester is used to calibrate the wrench to the torque level which will achieve the specified tension.
SD DOT
Notes: A sample of bolts to be used in the connections are tested to determine the torque level required to achieve the correct tension.
For calibrated wrench pretensioning, this testing shall be performed daily for the calibration of the installation wrench.
A more recent restriction is that the calibrated wrench can only be used where the nut is the turned element.
https://www.skidmore-wilhelm.com/

## Slide 33: Methods of bolt installation
Why do we consider pretensioning rather than torqueing the bolt?
Bolts are tightened in order to achieve some level of pretension on the bolt
Torque is a by-product in order to achieve proper tension – it is the twisting force that occurs when the nut and bolt are tightened.
Notes: Further discussion of Calibrated Wrench pretensioning in 8.2.2 of RCSC.

## Slide 34: Methods of bolt installation
Why do we consider pretensioning rather than torqueing the bolt?
Torqueing is difficult to measure accurately because of variation in factors such as:
- finish & tolerance on bolt and nut threads
- uniformity, degree and condition of lubrication.
- dust / dirt / corrosion of threads
The Calibrated Wrench Method, which uses torque to achieve pretension, requires daily calibrations in order to ensure verified torque-to-pretension relationships.

## Slide 35: Methods of bolt installation
Twist-Off Tension Control Bolts
F1852 and F2280 bolts are twist-off-type tension- control bolts
Notes: The bolts need to be snug tightened before twisting off and they need to be twisted off in a pattern from the most rigid part of the joint.

## Slide 36: Methods of bolt installation
Twist-Off Tension Control Bolts
These bolts must be pretensioned with a twist-off-type tension-control bolt installation wrench that has two coaxial chucks
Notes: Photo Courtesy of Jim Swanson, University of Cincinnati

## Slide 37: Methods of bolt installation
Twist-Off Tension Control Bolts
Shear stress is induced in the groove due to the opposing torques. The torque required to shear-off the spline is calibrated to the torque required to induce proper pretension in the bolt.
Notes: Tension-control bolts, ASTM F1852, are fasteners that meet the overall requirements of ASTM A325 bolts, but which have special features that pertain to their installation. In particular, the bolt has a splined end that extends beyond the threaded portion of the bolt and an annular groove between the threaded portion of the bolt and the splined end. The bolt shown has a round head (also called button or, dome, head), but it can also be supplied with the same head as heavy hex structural bolts. The bolt, nut, and washer must be supplied as an assembly, or, "set."
The special wrench required to install these bolts has two coaxial chucks—an inner chuck that engages the splined end and an outer chuck that envelopes the nut. The two chucks turn opposite to one another to tighten the bolt. At some point, the torque developed by the friction between the nut and bolt threads and at the nut–washer interface overcomes the torsional shear resistance of the bolt material at the annular groove. The splined end of the bolt then shears off at the groove. If the system has been properly manufactured and calibrated, the target bolt pretension is achieved at this point. Factors that control the pretension are bolt material strength, thread conditions, the diameter of the annular groove, and the surface conditions at the nut–washer interface. The installation process requires just one person and takes place from one side of the joint only, which is often an economic advantage. The wrench used for the installation is electrically powered, and this can be advantageous in the field.
Research that investigated the pretension of production tension-control bolts as it varied from manufacturer to manufacturer and under different conditions of aging, weathering, and thread conditions is available. The results show that the pretension in a tension control bolt is a strong reflection of the friction conditions that exist on the bolt threads, on the nut face, and on the washers supplied with the bolts. In this study, the quality of the lubricant supplied by the manufacturer varied, and in many cases the effectiveness of the lubricant decreased with exposure to humidity and the elements.
The installation of a tension-control bolt uses a method that depends on torque. As such, the process should be subject to the same pre-installation procedure demanded of calibrated wrench installation. Indeed, this is the requirement of the RCSC Specification. If calibration is carried out in accordance with that Specification, it is reasonable to expect that the bolt pretensions from tension-control bolts will be similar to those reported for calibrated wrench installation.
Source: AISC Design Guide 17
The bolt can only be tightened from the nut side. The spline adds length to the bolt. So these require more clearance than Hex bolts. This may prevent their use in skewed or tight conditions.
Note that specific and proper lubrication of “tension-control” or twist-off bolts is essential to the reliable installation of these fasteners.

## Slide 38: Methods of bolt installation
Direct Tension Indicators (DTI)
ASTM F959 DTI washers may also be used during pretensioning.
DTI Washers have protrusions that bear against the unturned element
As the bolt is tightened, the clamping force flattens the protrusions. A feeler gage is used to measure the gaps.
Notes: Installation of high-strength bolts to target values of bolt pretension can also be carried out using direct tension indicators. These are washer-type elements, as defined in ASTM F959 and shown in the figure, that are placed under the bolt head or under the nut. As the nut is turned, small arch-shaped protrusions that have been formed into the washer surface compress in response to the pretension that develops in the bolt. If a suitable calibration has been carried out, the amount of pretension in the bolt can be established by measuring the size of the gap remaining as the protrusions close. This calibration requires that a number of individual measurements be protrusions in the direct tension indicating washer used with a 7/8 in. dia. A325 bolt. There must be at least three feeler gage refusals at the target value of the gap, which is 0.015 in. Details of the direct tension indicating washer itself and the procedure necessary for calibration are given in the RCSC Specification and in the ASTM Standard. Over and above the particularities of the direct tension indicating washer itself, the verification process is similar to that for calibrated wrench installation.
The use of the load-indicating washer to install high-strength steel bolts is a deformation method of control, and so it is not subject to the friction-related variables that are associated with the calibrated wrench and tension control bolt methods. If the direct tension indicators are used in accordance with the requirements given in the RCSC Specification the bolt pretensions that are produced can be expected to be satisfactory.
Source: AISC Design Guide 17
These need to be snug-tight before pretensioning and need to be pretensioned in a pattern from the most rigid part of the connection.

## Slide 39: Bolt Dimensions
Notes: These dimensions are governed by ASME B18.2.6.
There are now both fix spline and twist-off spline; the difference is a groove called a shear collar between the end of the thread and the spline on twist-off bolts (bottom left). That groove is not there in fixed spline bolts.

## Slide 40: Bolt Dimensions
Table 7-14 (continued)
Notes: This is the continuation of Table 7-14 from AISC Steel Construction Manual (15th edition).

## Slide 41: Nominal Bolt Area
d
Notes: AISC uses nominal area and a reduction factor for thread loss where appropriate. This is conservative and more so for big bolts so we just added a footnote permitting the use of net tension area without the reduction factor.

## Slide 42: Bolt Length
  Bolt length depends on grip length, washer thickness, nut height and stick-through
  Sufficient Thread Engagement: having the end of the bolt, not including the spline of a spline-end bolt, or the available bolt threads extending beyond or at least flush with the outer face of the nut; a condition that develops the strength of the bolt
Notes: The length of the bolt is not dictated by the engineer. The important thing that engineers really need to know about length is that short bolts need to be designed as type N (threads included), as the threads of short bolts would need to be included along the shear plane.
The definition of “sufficient thread engagement” was added in RCSC 2020.

## Slide 43: Bolt Length
Notes: The threaded region be at least flush with the nut, or stick-through by some distance beyond the nut. The bolt can not end within the depth of the nut.

## Slide 44: Bolt Length
RCSC 2020
Notes: To determine the required bolt length, the value shown in Table C-2.2 should be added to the grip (i.e., the total thickness of all connected material, exclusive of washers). For each ASTM F436 washer that is used, add 5 /32 in.; for each beveled washer, add 5/16 in. The tabulated values provide for manufacturing tolerances and sufficient thread engagement with a heavy hex nut. The length determined by the use of Table C-2.2 should be adjusted to the nearest 4-in. increment (or 2-in. increment for lengths exceeding 6 in.). A more extensive table for bolt length selection based upon these rules is available (Carter, 1996; Swanson et al., 2020a).
Source: RCSC 2020
Carter, C.J. (1996), “Specifying Bolt Length for High-Strength Bolts,” Engineering Journal, Vol. 33, No. 2 (2nd Qtr.), AISC, Chicago, IL.
Swanson J.A., Rassati G.A., and Larson, C.M. (2020a), “Dimensional Tolerance and Length Determination of High-Strength Bolts,” Engineering Journal, Vol. 57, No. 1 (1st Qtr.), AISC, Chicago, IL.

## Slide 45: Bolt Length
RCSC 2020
Notes: Structural bolts are manufactured to the dimensions specified in ASME B18.2.6.

## Slide 46: Bolt Length
Notes: Bolt length is the length of the shank (not including the bolt head) and it can be calculated using this table. It includes the sum of the grip (connecting surfaces), washer thickness, and the additional value in the table. This table value considers the nut depth and necessary stick-through.

## Slide 47: Bolt Length
  Specify X bolts if designing with threaded eXcluded
  Specify N bolts if designing with threads iNcluded

## Slide 48: Bolt Holes
  Standard
  Short-slot
  Long-slot
  Oversize
Notes: The use of oversized or slotted holes can be of great benefit to erectors because their use allows more tolerance when placing the components of the assembly. The question to be addressed here is the effect that oversized or slotted holes might have upon the expected performance of the connection.
The standard hole size for high-strength bolts is 1/16 in. greater than the nominal diameter of the bolt to be used. Particularly in joints that have many bolts, it is possible that not all holes in one component will line up exactly with the holes in the mating material. However, if oversized holes are used, omni-directional tolerance exists. If slotted holes are used, a greater tolerance is provided than for oversized holes, but this tolerance is mainly in one direction, the direction of the slot. The effect of oversized or slotted holes upon net section is taken into account directly in the design calculations because the oversized hole or slot dimensions will be used. Therefore, the concern becomes one relating to the bolt behavior—will the bolt in a slotted hole or an oversized hole be reduced in capacity as a consequence.
For the case of snug-tightened joints only, when slotted or oversized holes are used in an outside ply, either an ASTM F436 washer or a 5/16 in. thick common plate washer is required. If the joint is either pretensioned or slip-critical, then washer requirements reflect the fact that intended bolt pretensions may not be attained with standard washers.
Tests have shown that both oversized and slotted holes can significantly affect the level of preload in the bolt when standard installation procedures are used. Consider an oversized hole, for example. As a hole becomes larger relative to the bolt diameter, the amount of material remaining to react the force in the bolt is reduced. Consequently, the connected material around the periphery of the hole is under higher contact stresses than would otherwise have been the case. This is exacerbated if the bolt head, nut, or washer actually scours the connected material. The situation is similar when slotted holes are used. As a result, the amount of bolt elongation (and, pretension) for a given turn-of-nut will be less than if a standard hole were present.
Tests have shown that using standard washers, which are 5/32 in. thick, often does not permit the expected bolt pretensions to be attained when oversized or slotted holes are used. A greater washer thickness (i.e., stiffness) is required to bridge the opening and enable the delivery of normal pretensions.
Source: AISC Design Guide 17

## Slide 49: Bolt Holes
Notes: Holes detailed larger than those shown in the table are permitted when specified or approved by the Engineer of Record.
Oversized holes, short slots not perpendicular to the applied load, and long slots in any direction shall be subject to approval by the Engineer of Record. Any restrictions on the use of hole types shall be specified in the design documents.

## Slide 50: Methods of making bolt holes
  AISC Specification regarding method of making holes is based on performance criteria:
  Bolt holes shall comply with the provisions of the RCSC Specification for Structural Joints Using High-Strength Bolts Section 3.3…except that thermally cut holes are permitted with a surface roughness profile not exceeding 1,000 μin. (25 μm), as defined in ASME B46.1. Gouges shall not exceed a depth of 1 /16 in. (2 mm). Water jet cut holes are also permitted.
Notes: Fabricator used to have two ways to make holes: drilling and punching. With CNC cutting, any plate with a reentrant corner will be cut on a CNC burning table and so it is typical to just burn the holes as well at that time. While each hole might take a little longer to burn, the cutting of the plate, layout of the holes, and cutting the holes is faster if done in one operation. Thermal cutting of holes became desirable and AISC wrote quality requirements to permit it. The same is true for water jet and laser.

## Slide 51: Methods of making bolt holes
  RCSC 2020
Notes: Here is the criteria for bolt holes per RCSC 2020. It provides a tolerance on dimensions that is 1/32”. RCSC 2014 table is very similar.
RCSC 3.3 also states: Burrs less than or equal to 1/16 in. in height are permitted to remain on faying surfaces of all joints. Burrs larger than 1/16 in. in height shall be removed or reduced to 1/16 in. or less from the faying surfaces of all joints.

## Slide 52: Methods of making bolt holes
  Possible methods include:
  Punching*
  Subpunching and reaming
  Drilling*
  Hole sawing
  Laser cutting
  Thermal cutting, subject to surface quality requirements *
  Water jet cutting
  * typical
Notes: The Specification previously limited the methods used to form holes, based on common practice and equipment capabilities. Fabrication methods have changed and will continue to do so. To reflect these changes, this Specification has been revised to define acceptable quality instead of specifying the method used to form the holes, and specifically to permit thermally cut holes. AWS C4.1, Sample 3, is useful as an indication of the thermally cut profile that is acceptable. The use of numerically controlled or mechanically guided equipment is anticipated for the forming of thermally cut holes. To the extent that the previous limits may have related to safe operation in the fabrication shop, fabricators are referred to equipment manufacturers for equipment and tool operating limits.
Source: AISC 360-16, Chapter M Commentary

## Slide 53: Bolt Holes
  Standard
  Standard Holes
  For bolts < 1”, db + 1/16”
  For bolts ≥ 1”, db + 1/8”
  Most common hole type

## Slide 54: Bolt Holes
  Oversize Holes
  Bolt holes are up to 5/16” greater than bolt size
  Larger holes allow for ease of fit up
  Permitted in slip-critical connections but not used in bearing-type connections
  Oversize
Notes: For snug-tightened or pretensioned joints subject to shear or combined shear and tension, oversized holes are not permitted. In such joints subject to tension only, oversized holes are permitted upon approval by the Engineer of Record.
Source: RCSC 2020, Chapter 3

## Slide 55: Bolt Holes
  Short-Slot Holes
  Hole width is standard hole dimension
  Hole length is a short slot
  Slot allows for ease of fit up along hole length
  Permitted in slip-critical or bearing- connections.
  To use in bearing connection, load must be normal to the length of the hole
  Short-Slot (SSL)
  width
  length
Notes: For snug-tightened or pretensioned joints, short-slotted holes are permitted in only one ply at any individual faying surface of any joint, provided the applied load is approximately perpendicular (between 80 and 100 degrees) to the axis of the slot. When complete connection design is not shown in the structural design drawings, the Engineer of Record shall be notified when short-slotted holes are used in this manner.
For snug-tightened or pretensioned joints, upon approval by the Engineer of Record, short-slotted holes are permitted in more than one or all plies, provided the applied load is approximately perpendicular (between 80 and 100 degrees) to the axis of the slot(s).
Source: RCSC 2020, Section 3

## Slide 56: Bolt Holes
  Long-Slot Holes
  Hole width is standard hole dimension
  Hole length is a long slot
  Slot allows for ease of fit up along hole length
  Permitted in only one of the connected parts of either a slip-critical or bearing-type connection at an individual faying surface
  Long-slotted holes are permitted without regard to direction of loading in slip-critical connections, but shall be normal to the direction of loading in bearing-type connections.
  Long-Slot (LSL)
  width
  length
Notes: For snug-tightened or pretensioned joints, upon approval by the Engineer of Record, long-slotted holes are permitted in only one ply at any individual faying surface, provided the applied load is approximately perpendicular (between 80 and 100 degrees) to the axis of the slot.
For slip-critical joints, upon approval by the Engineer of Record, long-slotted holes are permitted in only one ply at any individual faying surface, without regard for the direction of the applied load.
Source: RCSC 2020, Section 3

## Slide 57: Bolt Holes
  Holes are made by drilling, punching, or thermal cutting
  Method of choice is left to the fabricator
  Depends on material thickness and what other operations are performed on the piece
Notes: Rivets and bolts are used in drilled, punched, or flame-cut holes to fasten the parts to be connected. Can also be sub-punched and reamed.
Thermally cut holes produced by mechanically guided means are permitted in statically loaded joints.
Slotted holes in statically loaded joints are often produced by punching or drilling the hole ends and thermally cutting the sides of the slots by mechanically guided means. The sides of such slots should be ground smooth, particularly at the junctures of the thermal cuts to the hole ends.
Source: RCSC 2020, Section 3

## Slide 58: Bolt Holes
  Hole Dimensions for Calculations
  For hole-related limit states (i.e. – net area calculations), the width of the bolt hole shall be taken as 1/16 in. greater than the nominal dimension of the hole:
  d’ h = dh + 1/16 in.
  (AISC Comm. B4.3b)
  The additional 1/16 in. accounts for damage around hole during drilling or punching operations.
  When calculating net area, 1/16 in. should be added to the nominal hole dimension from Table J3.3.

## Slide 59: Minimum spacing
  Distance between centers of holes (spacing, s) shall not be less than times the nominal diameter, d, of the fastener.
  Clear distance between bolt holes or slots shall not be less than d.
  Distance of 3d between centers of standard, oversize, or slotted holes is preferred.
Clear distance
Spacing, s
(AISC 360 – Section J3.3)
Notes: The minimum spacing dimension of 2 2/3 times the nominal diameter is to facilitate construction and does not necessarily satisfy the bearing and tearout strength requirements in Section J3.10.
The preference of 3d is a user note in Section J3.3.

## Slide 60: Minimum Edge Distance
  Edge distance in any direction shall not be less than Table J3.4, or as required in Section J3.10.
  Edge distance of oversized or slotted hole shall be not less than that required for a standard hole to an edge of a connected part plus the applicable increment, C2, from Table J3.5.
Edge distance
Edge distance
(AISC 360 – Section J3.10)
Notes: Prior to the 2010 AISC Specification (AISC, 2010), separate minimum edge distances were given in Tables J3.4 and J3.4M for sheared edges and for rolled or thermally cut edges. Sections J3.10 and J4 are used to prevent exceeding bearing and tearout limits, are suitable for use with both thermally cut, sawed and sheared edges, and must be met for all bolt holes. Accordingly, the edge distances in Tables J3.4 and J3.4M are workmanship standards and are no longer dependent on edge condition or fabrication method.
Source: AISC 360-16, Chapter J Commentary

## Slide 61: Minimum Edge Distance
  Table J3.4 edge distances are minimum edge distances based on standard fabrication practices/workmanship tolerances.

## Slide 62: Minimum Edge Distance

## Slide 63: Maximum spacing and Edge Distance
  Maximum edge distance to the nearest edge shall be 12 times the thickness of the connected part under consideration, but shall not exceed 6 in.
  Maximum bolt spacing:
      (a) For painted members or unpainted members not subject to corrosion, the spacing shall not exceed 24 times the thickness of the thinner part or 12 in.
      (b) For unpainted members of weathering steel subject to atmospheric corrosion, the spacing shall not exceed 14 times the thickness of the thinner part or 7 in.
(AISC 360 – Section J3.5)
Notes: Limiting the edge distance to not more than 12 times the thickness of the connected part under consideration, but not more than 6 in. (150 mm), is intended to provide for the exclusion of moisture in the event of paint failure, thus preventing corrosion between the parts that might accumulate and force these parts to separate. More restrictive limitations are required for connected parts of unpainted weathering steel exposed to atmospheric corrosion.
The longitudinal spacing applies only to elements consisting of a shape and a plate, or two plates. For elements, such as back-to-back angles not subject to corrosion, the longitudinal spacing may be as required for structural requirements.
Source: AISC 360-16, Chapter J Commentary

## Slide 64: 2- Connection Basics: Bolts and Welds
Bolts
  Bolt grades
  Bolt connection types
  Bolt installation methods
  Bolt sizes and hole sizes
  Dimensional limitations
Welds
  Weld processes
  Weld types
  Dimensional limitations
  Weld Symbols
Notes: Now we will talk about basics of welds: helpful resources, the processes, weld types, dimensional limitations and weld symbols.

## Slide 65: Welds – helpful resources
AISC Specification - Chapter J Design of Connections*
American Welding Society (AWS) D1.1 – Structural Welding - Steel
AWS D1.5 – Bridge Welding Code
AWS D1.8 – Structural Welding Code – Seismic Supplement
AISC Manual Part 8 – Design Considerations for Welds
AISC Design Guide 21: Welded Connections - A Primer for Engineers +
* available for a free download from AISC.org or boltcouncil.org
+ available for free from AISC.org with free AISC Student Membership
Notes: The PDF versions of all AISC Design Guides are available for free download by AISC Educator and Student Members at https://www.aisc.org/publications/design-guides/design-guide-pdfs
Note: When students purchase a Steel Construction Manual through the Manual Discount Program, they are automatically enrolled as AISC Student Members.

## Slide 66: Welds - Definition
“A localized coalescence of metals or nonmetals produced by heating the materials to the welding temperature, with or without the application of pressure, or by the application of pressure alone and with or without the use of filler material.”
(AWS A3.0)
In arc welding, heat is always applied, although pressure typically is not. All arc welding processes involve melting of the metals being joined and require shielding.

## Slide 67: Welds - definition
Shielding
Shielding keeps nitrogen and oxygen in the environment from reacting with the molten metal and causing bubbles, embrittlement
Typically accomplished by flux and/or gases
  Flux forms slag that coats/shields the droplets
  Inert gases (such as argon or helium) or gas such as carbon dioxide is generated from fluxes or gas delivered directly to the weld region - these gases move nitrogen and oxygen away from the region
Notes: Molten metal, like the weld pool, has the ability to dissolve large quantities of gases such as nitrogen and oxygen. As the metal cools, the solubility of these gases in the liquid metal decreases, and dissolved gases precipitate out or, alternatively, react with metallic atoms, forming various nitrides and oxides. When this evolution of gas occurs near the solidification temperature, the gas bubbles exiting the liquid metal can leave behind spheres or cylindrical cavities, just as the metal solidifies. Such volumetric voids in the weld metal are called porosity. Additionally, small quantities of nitrogen left behind in the metal can cause embrittlement, even if no porosity is present. Metallic compounds can combine with nitrogen and oxygen to form inclusions and reduce mechanical properties. Given that the atmosphere is composed of roughly 80 percent nitrogen and 19 percent oxygen, both the weld pool and the drops of metal that leave the electrode must be protected from these gases.
Shielding is typically accomplished by one of two means, or a combination of both. Fluxes melt to form slags, which may be used to coat the individual droplets of metal that leave the electrode. Additionally, once the slags contact the weld pool, they float to the surface and shield the pool as well. Slags act as a mechanical lid on the weld pool, keeping nitrogen and oxygen from contaminating the weld deposit. Additionally, such slags perform another important function: For out-of-position welding (vertical, overhead), the slag constitutes a mechanical support for the liquid weld metal, helping to shape the weld bead and hold it in place.
The second means of shielding is through gases. Such gases may be generated from fluxes contained in, on, or around the electrode, or shielding gas may be delivered directly to the weld region. Suitable shielding gases include inert gases, such as argon and helium, or carbon dioxide, which is not inert but is sufficient for shielding nonetheless. These gases displace the atmosphere, moving nitrogen and oxygen away from the region.
Source: AISC Design Guide 21

## Slide 68: WelD Processes
SMAW: Shielded Metal Arc Welding
FCAW: Flux-cored Arc Welding
SAW: Submerged Arc Welding
GMAW: Gas-Metal Arc Welding
Structural welding is a process by which the parts that are to be connected are heated and fused, with supplementary molten metal at the joint.
Notes: Currently, in the fabrication and erection of steel buildings, three welding processes dominate. These processes, plus a few others that are occasionally used for specialized applications, will be covered in this section. All involve melting and mixing of filler metals and base metals, followed by solidification and fusion of the various materials. “Arc welding” defines a group of welding processes that involve heating the work pieces with an electric arc.
The choice of welding process is usually left up to the contractor, as the contractor is typically best positioned to select the optimal process for a given application. In unique situations, the engineer may specify a special process, or processes for specific applications in the contract documents, but this practice is uncommon. The selection of the welding process is typically considered part of the “means and methods” of construction, and the choice of process may significantly affect the cost of a project. When properly used, all of the welding processes listed in AWS D1.1 are capable of delivering welds with the requisite quality for building construction. Of course, any welding process can be abused, and all can produce welds of poor quality if improper procedures are used, or if the welder’s skills are inadequate.
Although the selection and control of the welding process is typically the responsibility of the contractor, it is important that all parties involved understand these processes in order to ensure high quality and economical fabrication. Particularly when problems arise on a project, the engineer may be required to become involved with welding process issues, and a basic knowledge of how the process operates will aid in resolving construction problems.
Source: AISC Design Guide 21

## Slide 69: WelD Processes
SMAW: Shielded Metal Arc Welding
Notes: In shielded metal arc welding (SMAW), commonly known as “stick” welding or manual welding, an arc is established between a coated electrode and the weld pool. Shielding for the process is supplied by the electrode coating, which decomposes as the filler metal is consumed.
Metal from the metallic core of the electrode is melted and becomes part of the deposited weld. SMAW is the successor to bare metal arc welding, which relied only on a light coating on the electrode and was essentially unshielded. With the addition of the flux coating on the electrode, weld quality was significantly enhanced.
SMAW is characterized by versatility, simplicity, and flexibility. In the 1940s, 1950s and 1960s, SMAW was commonly used for field erection of steel buildings, as well as for shop fabrication that could not be done with submerged arc welding. The advent of flux cored arc welding in the 1960s, however, displaced much of the SMAW in both the shop and field.
SMAW is commonly used for tack welding, fabricating miscellaneous components, and repair welding. It has earned a reputation for dependably depositing high-quality welds. It is, however, slower and more costly than other methods of welding. In order to obtain quality welds, more welder skill is typically required for SMAW as compared to the semi-automatic processes. SMAW is one of the prequalified processes listed in AWS D1.1 and the WPS used with this process can be prequalified, providing all the criteria of AWS D1.1, clause 3, are met.
(Note: WPS is welding procedure specification. For a WPS to be prequalified, it must comply with all the provisions of the code including prequalified steels, filler metals, preheat levels, weld joint details, welding processes, and welding parameters. If not prequalified, it has to be tested. The limits and tests are described in Clause 3 of AWS D1.1.)
Process Issues & Concerns for the Engineer: Some electrodes for SMAW are referred to as low hydrogen while others are not. Because both types of electrodes are available and because the use of electrodes that are not low hydrogen may lead to cracking, it is important to know the differences in these filler metals and where low-hydrogen electrodes are required. AWS D1.1 addresses the acceptability of these electrodes for prequalification welding procedure specifications (WPS).
Source: AISC Design Guide 21

## Slide 70: WelD Processes
SMAW: Shielded Metal Arc Welding
Notes: SMAW welding is performed using a power supply with constant current (CC) output (Figure 2–3, DG 21). Formerly, this was called variable voltage (VV). Either alternating current (AC) or direct current (DC) may be used. If primary electrical power is available, a transformer (for AC output) or a transformer/rectifier (for DC output) is used to convert the high-voltage alternating current into high-amperage output, suitable for welding. Today, small, lightweight, and highly portable inverter power supplies can perform this function more efficiently, reducing operating costs. When primary power is not available, the same type of equipment may be powered by portable power generation systems. Alternatively, individual engine-driven welders, fueled by gasoline, diesel fuel, or propane, can be used to generate the necessary welding power directly.
Electrodes for SMAW consist of a solid-core wire, surrounded by a coating of material called flux. The materials vary in composition, but the purpose of all coatings is to shield the molten weld metal from the atmosphere. After this function is complete, the decomposed coatings form a slag coating that covers the final weld. The slag is removed after welding. One end of the electrode has no coating; this is the grip end where the exposed core wire is inserted into the electrode holder. The size of the electrode is based upon the diameter of the core wire. Electrodes range in size from 1/8 in. to 3/16 in. for most structural work, although smaller and larger sizes are available. Larger electrodes can carry more welding current, and thus melt faster, yielding higher production rates. The as-received lengths of the electrodes vary with the diameter and an electrode that is 14 to 18 in. long is typical (Figure 2–5, DG21).
Today, SMAW is seldom used for the primary shop fabrication or field erection of buildings due to its lower productivity. However, because of its simplicity, it is used where access for equipment is limited or when transporting and positioning of equipment would be a major task. A prime example is tack welding—moving equipment around a structural component may take more time than making the tack welds. Thus, SMAW is often used for this purpose. Portability makes SMAW ideal for applications such as welding sheet steel decks to supporting members.
The flexibility of SMAW may make it the contractor’s process of choice where a whole range of welds must be made. This is often the case for smaller field erection projects where a limited number of welders may be used to make a variety of welds. Repair welds are often made with SMAW, again due in part to its flexibility.
The chief disadvantage of SMAW lies in its inherently lower productivity rate, and thus it is not typically used for large, long welds, which are better performed with more automated welding processes.
Source: AISC Design Guide 21
Size usually indicates diameter of the core rod. Common from 1/8 to 7/32 inch.

## Slide 71: WelD Processes
FCAW: Flux-Cored Arc Welding
Notes: Flux-cored arc welding (FCAW) is “an arc welding process using an arc between a continuous filler metal electrode and the weld pool. The process is used with shielding gas from a flux contained within the tubular electrode, with or without additional shielding from externally supplied gas, and without the application of pressure” (AWS, 2010). Inside the tubular electrode is a combination of materials that include flux and perhaps metal powders. The flux ingredients inside the electrode perform the same function as the flux on the outside of an SMAW electrode and eventually form an extensive slag cover over the weld bead. FCAW electrodes are said to be “continuous.” In reality, they have finite length, but because these wire electrodes are spooled onto packages that may consist of anywhere from 1 to 1,000 lb of material, they are virtually continuous in comparison to SMAW electrodes.
FCAW may be applied automatically or semi-automatically, although most FCAW is done semiautomatically. In semiautomatic welding, the welded holds the gun and controls travel speed, whereas in automatic welding, these functions are mechanically controlled. With SMAW, the welder must maintain the arc length (the gap between the electrode and the workpiece), while manually feeding the electrode into the puddle and advancing the electrode along the joint. With automatic and semiautomatic processes such as FCAW, the operator does not need to maintain the arc length or feed the electrode into the puddle. The power supply maintains the arc length and the wire feeder delivers the electrode to the arc. In automatical welding, the travel speed is regulated by a mechanism that advances the electrode along the joint.
Process Issues & Concerns for the Engineer: Certain flux-cored arc welding (FCAW) electrodes are intended to be used for making single-pass welds. When misapplied and used in multiple-pass applications, such electrodes may induce cracking. AWS D1.1 precludes the use of these electrodes for prequalified WPS.
Source: AISC Design Guide 21

## Slide 72: WelD Processes
FCAW: Flux-Cored Arc Welding
Notes: Within the category of flux-cored arc welding, there are two specific subsets: gas-shielded flux core (FCAW-G) and self-shielded flux core (FCAW-S). Self-shielded flux-cored electrodes require no external shielding gas; the entire shielding system results from the flux ingredients contained within the core of the tubular electrode. The gas-shielded versions of flux-cored electrodes utilize an externally supplied shielding gas. Self-shielded flux-cored electrodes are better suited for field welding situations where wind may displace the shielding gas required for FCAW-G. The FCAW-G process tends to be more operator friendly and is generally preferred in situations where the gas shielding can be protected from disruption.
FCAW is one of the prequalified processes listed in AWS D1.1, and the WPS used with this process can be prequalified, provided that all of the criteria of AWS D1.1, clause 3 are met.
Note: This slide is showing self-shielded wire. Gas shielded is typically used in the shop and self-shielded used in the field. Self-shielded permits welding without having to bring gas to the field.
The flux cored arc welding process offers two distinct advantages over shielded metal arc welding. First, the electrode is continuous, eliminating the built-in starts and stops that are inevitable with shielded metal arc welding. Not only does this have an economic advantage because the welder can continue welding until the weld is complete, but arc starts and stops, which create potential sources of weld discontinuities, are reduced.
The second major advantage is that increased amperages can be used with flux cored arc welding, with a corresponding increase in deposition rate and productivity. While the gun cable assembly may be 10 or more ft long, the electrical power is delivered to the tubular electrode near the point where it exits the gun. As the electrode passes through a hollow copper tube, called a contact tip, the electrical energy is transferred to the electrode. Then, current is transferred through the electrode until it gets to the arc.
The short distance from the contact tip to the arc is known as the electrode extension or “stickout” and is typically w ¾ in. to 1 1/8” in., although it may be as large as 2 or 3 in. Given that this distance is small, and that the electrode is typically fed through the contact tip at a rate of 200 in. per minute or more, there is little time for the electrode to overheat. The higher permissible amperages allow for higher deposition rates (i.e., more pounds of metal can be deposited in a given length of time). Additionally, because of the continuous electrode, the arc can stay lit longer since there is no interruption to change electrodes. Combined, these two features make FCAW much more economical to use as compared to SMAW.
Because FCAW is semi-automatic, welders do not need to maintain the arc length—that is controlled by the machine. However, the welder must maintain the electrode extension or “stickout” distance. The welder does not need to feed the filler metal into the joint — that is done by the wire feeder. Unlike the variable resistor associated with SMAW, FCAW has a fixed resistance (for a given electrode extension), and more uniform welding conditions are maintained. In some ways, less welder skill is required for FCAW welding. However, because of the higher deposition rates involved, FCAW welders must learn how to control the larger volumes of molten metal that are common to this process.
FCAW welding equipment costs more and is less portable than SMAW equipment. Guns and cables are more costly to buy and maintain than are the simple electrode holders used for SMAW. To change from one size of electrode to another, the welder has to change the coil or spool of electrode, perhaps change the drive rolls in the wire feeder, and make changes to the gun and cable assembly. Thus, as compared to SMAW, such changes are more complicated.
Source: AISC Design Guide 21

## Slide 73: WelD Processes
SAW: Submerged Arc Welding
Notes: For shop welding, an automatic or semi automatic process is usually used. SAW is one possible process.
Submerged arc welding (SAW) is “an arc welding process using an arc or arcs between a bare metal electrode or electrodes and the weld pool. The arc and molten metal are shielding by a blanket of granular flux on the workpieces. The process is used without pressure and with filler metal from the electrode and sometimes from a supplemental source.” (AWS, 202)
Because the arc is completely covered by the flux (i.e. it is submerged), it is not visible and the weld is made without the flash, spatter and sparks that characterize the open-arc processes. The nature of the flux is such that little smoke or visible fumes are emitted under normal conditions.
SAW is typically used automatically, although semiautomatic operation is also utilized. In automatic welding, the electrode is positioned with respect to the joint and also is automatically propelled along the length of the joint, as shown in the figure on the next slide.
SAW is most commonly used with one electrode, although it is possible to use more. Two electrodes may be fed through a single electrical contact tip, and this is formally called parallel electrode welding. When two or more separate, individually controlled arcs are used, the configuration is formally known as multiple electrode welding, although it is often called tandem arc welding. The granular flux must stay in place to shield the weld pool, and thus, SAW is restricted to the flat and horizontal welding positions.
Like FCAW, SAW equipment consists of a power source, a wire feeder, a device through which the electrode is fed and electrical power is introduced, and a work lead and clamp. The power supply can be either constant current or constant voltage, and SAW can be performed with either direct or alternating current. In the more common automatic mode, the electrode is propelled along the joint in a mechanized system, or the work is moved under a fixed welding head. In semi-automatic welding, the welder moves the gun along the joint. The mechanized systems range from simple systems that move a semi-automatic gun along the joint to self-contained wire-feeder/motion-control systems typically called tractors. Welding fixtures are typically required when the work is moved under a fixed head, and such systems may become quite large and complex, depending on the nature of the work being done.
SAW additionally requires a flux delivery system. For many applications, a simple hopper allows the flux to be delivered by gravity. For semi-automatic applications, a pressurized container is used, and the flux is delivered by means of compressed air, which must be clean and dry, or the flux will become contaminated. Multiple-electrode SAW refers to a variation of submerged arc that utilizes at least two separate power supplies and two separate wire drives, and feeds two electrodes independently. Some applications, such as the manufacture of line pipe, may use up to five independent electrodes in a multiple-electrode configuration.
Additional Note: Welds melt into the base metal and AISC and AWS permit designers to use that extra throat if the contractor can show that it is consistent. SAW is a good candidate for this because it runs hotter than SMAW or FCAW so it often penetrates more. So the weld can be stronger but the weld metal is the same design strength.
Source: AISC Design Guide 21

## Slide 74: WelD Processes
SAW: Submerged Arc Welding
Notes: SAW is capable of high productivity rates because it can use higher welding currents, resulting in higher deposition rates and deeper penetration. Higher deposition rates simply mean that the contractor can deposit the required weld in less time. The deeper penetration may allow fillet-weld sizes to be reduced, or may permit the use of groove-weld details that require less weld metal. For even higher deposition rates, a second or third electrode can be added into the system to increase productivity further. Because the process typically is automated, SAW welds usually are made continuous for the length of the joint.
Welds made under the protective layer of flux are excellent in appearance and spatter-free. This is of particular significance for steel designated as architecturally exposed structural steel (AESS) where the completed SAW weld rarely requires any post-weld treatment to enhance its appearance.
Another benefit of the SAW process is freedom from the open arc. This means that the welder is not required to use the standard protective helmet, and multiple welding operations can be conducted in a tight, restricted area without the need for extensive shields to guard the operators from arc flash. The process produces very little smoke, which is another production advantage, particularly in situations with restricted ventilation. The freedom from the open arc also proves to be one of the chief drawbacks of the process; it does not allow the operator to observe the weld puddle. When SAW is applied semi-automatically, the operator must learn to propel the gun carefully in a manner that will ensure uniform bead contour. The experienced operator relies on the formation of a uniform slag blanket to indicate the nature of the deposit underneath it. For single-pass welds, this is mastered fairly readily; however, for multiple-pass welding, the degree of skill required is significant. Therefore, most submerged arc applications are mechanized.
The nature of the joint must then lend itself to automation if the process is to prove viable. Long, uninterrupted, straight seams are ideal applications for SAW. Short, intermittent welds are better made with one of the open-arc processes.
Finally, SAW is restricted to the flat and horizontal position. For shop fabrication, the use of positioners, or simple reorientation of the weldment, can facilitate in-position welding. However, field conditions prohibit such opportunities, and thus restrict the suitability of SAW.
Because of its advantages, many fabricators will use SAW anywhere it is practical. Typical applications include the longitudinal seams on plate girders, box sections, and cruciform columns. In bridge shops, butt splices of flanges and webs are typically made with SAW, as are the stiffener-to-web welds.
Source: AISC Design Guide 21

## Slide 75: WelD Processes
GMAW: Gas-Metal Arc Welding
Notes: The gas metal arc welding (GMAW) process utilizes an arc between a typically solid electrode and the weld pool, with a shielding gas that surrounds the arc. The process and equipment are very much like FCAW-G. GMAW uses a solid- or metal-cored electrode and leaves no appreciable amount of residual slag. Historically, GMAW has not been a common method of welding in the structural steel fabrication shop because of its sensitivity to mill scale, rust, limited puddle control, and shielding loss. However, developments such as metal-cored electrodes and improved controls for pulsed GMAW are resulting in increased use of this process for structural steel.
GMAW has a variety of colloquial names, including the popular term MIG (metal inert gas) welding, and others such as mini-wire welding, micro-wire welding, and solid-wire welding. When GMAW is performed with carbon dioxide (CO2) shielding gas, it may be referred to as MAG (metal active gas) welding. The transfer of metal from the electrode to the weld pool may occur in several manners, called transfer modes. While a dozen or so transfer modes have been defined, four are commonly used in structural applications.
GMAW is one of the prequalified processes listed in AWS D1.1, and the WPSs used with this process can be prequalified, providing all the criteria of AWS D1.1, clause 3, are met. As an exception, GMAW-S (the short circuit transfer mode discussed below) may not be used with prequalified WPSs. GMAW-S is in the category of “code-approved” processes.
GMAW, like FCAW, requires a power supply, a wire feeder, a gun and cable system, a work lead and clamp, and a power lead that runs from the power source to the wire feeder. Some GMAW power supplies and wire feeders are combined into one self-contained housing. Additionally, a shielding gas regulator and flow meter, and hoses are required. GMAW is performed using a constant voltage (CV) power supply. The wire feeder mechanically drives the coiled electrode through the gun and cable system. Gun cable assemblies are typically 10 to 15 ft long, allowing for some movement of the gun from the wire feeder.
GMAW and FCAW equipment is similar enough that in many cases it is used interchangeably. GMAW power supplies may have additional controls for optimizing the output characteristics for certain modes of transfer.
GMAW, regardless of the mode of transfer, has some inherent advantages and limitations that will be presented first. Because no slag covers the weld, cleanup after welding is simple and low cost. GMAW electrodes typically cost less than flux-cored electrodes. GMAW has all the previously cited advantages of semi-automatic and automatic processes. GMAW with solid electrodes is capable of depositing weld metal with very low levels of diffusible hydrogen. An overall limitation of GMAW, regardless of mode, is that the process is more sensitive to contaminants that might be present on the steel surface, including mill scale, rust, and oil. GMAW can handle some of these contaminants, but other processes with slag systems can typically tolerate greater levels of such materials. Porosity may result when surfaces are too contaminated, and heavy scale may inhibit fusion.
As a gas-shielded process, GMAW has the same limitations as does FCAW-G: If the gas shield is disturbed, porosity will result. Even before the onset of porosity, the mechanical properties of the weld deposit, specifically the ductility and toughness, may deteriorate. Additional advantages and limitations of GMAW depend on the mode of transfer. Spray transfer permits higher deposition rates and deposits welds with good appearance, but requires the use of the higher cost argon-based shielding gas mixtures and can be used only in the flat and horizontal positions. Globular transfer uses low-cost carbon dioxide shielding and offers high deposition rates, but weld appearance is inferior to spray transfer, and extensive spatter is typical. The mode is also restricted to the flat and horizontal positions.
Short circuit transfer is ideal for sheet metal, and while it can be used out-of-position (vertical and overhead), the strong tendency toward fusion defects makes it undesirable for most structural applications.
Pulsed spray arc permits all-position welding and deposits welds with good appearance. Like spray transfer, this mode requires the use of the more expensive argon-based shielding gas mixtures. The welding equipment is more expensive and complex, but technical advances in power source controls have simplified the user interfaces.
GMAW is not widely used in the structural steel fabrication industry in the United States, but both solid and metal-cored electrodes have been used for shop fabrication of a variety of miscellaneous applications. Typically, but not exclusively, the welds are limited to single-pass situations. A major user of GMAW is the metal building industry, where nearly all semi-automatic welding is done with this process. Because it offers freedom from slag, GMAW is often used for tack welding.
Process Issues & Concerns for the Engineer: The mode of transfer describes the nature of the transfer of metal from the end of the electrode to the weld pool. Multiple modes of arc transfer are possible with gas metal arc welding (GMAW). One mode is short-circuit transfer, a low-energy mode of transfer that may lead to the weld defect of incomplete fusion. This is a serious defect that behaves much like a crack. Because the same electrode, equipment, shielding gas and other factors can be used for both short-circuit transfer and other modes of transfer, it is important to understand the conditions under which short-circuit transfer may occur. AWS D1.1 does not permit the use of short-circuit transfer with prequalified WPS, although the mode may be used when the WPS is qualified by test and the welder is qualified to use this mode.
Source: AISC Design Guide 21

## Slide 76: WelDing positions
Position of a joint during the welding process has a definite structural and economic significance
Position of joint affects:
  Ease of the weld
  Size of the electrode
  Current required
  Thickness of each weld layer deposited in multi-pass welds

## Slide 77: WelDing positions
Basic weld positions are:
Flat: face of weld is horizontal and welding performed from above
Horizontal: axis of weld is horizontal
Vertical: axis of weld is vertical
Overhead: welding performed from the underside of the joint

## Slide 78: WelDing positions
Horizontal Position
Overhead Position
Vertical Position
Flat Position
Notes: AWS D1.1 prescribes limits of angular deviation from true horizontal and vertical planes.
The flat position is preferred in all types of welding because weld metal can be deposited faster and easier. For example, a 5/16” fillet weld may require 50% more time to deposit in the horizontal position than in the flat position. Vertical & overhead welds may take three times as long as the same weld made in the flat position. In shop, the work is usually positioned to permit flat or horizontal welding by turning the members over as needed.
Source: AISC Detailing for Steel Construction

## Slide 79: Weld Types
Joint Types: affects the type of weld
Notes: These are different types of joint configurations that influence the type of weld to be specified.
i.e. – butt joints may use groove welds, lap joints may use fillet welds, etc.

## Slide 80: Weld Types
Primary Weld Types:
Notes: Welds may be placed into three major categories: groove welds, fillet welds, and plug/slot welds. For groove welds, there are two subcategories: complete joint penetration (CJP) groove welds and partial joint penetration (PJP) groove welds. Groove and fillet welds are of primary interest for major structural connections. The most common use of plug and slot welds in structural applications is for joining the center of large web doubler plates to deep wide-flange members (fillet welds are typically applied around the perimeter).
Source: AISC Design Guide 21

## Slide 81: Weld Types
Flare Bevel
Square Groove

## Slide 82: Weld types
Groove Weld Preparations
Notes: A variety of groove weld preparations are possible for CJP groove welds as shown. Preparations are necessary because, except for the thinnest of materials, the penetration of the welding processes is typically not adequate to obtain the depth of fusion required for the needed weld strength. Thinner sections, up to a maximum of 3/8 in., may be joined with square edge preparations using prequalified welding procedure specifications.
For most structural steel applications, therefore, some type of joint preparation is required. The easiest preparations to make and the most commonly applied involve planar surfaces, e.g., the V- and bevel-groove weld types. The curved surfaces associated with the U- and J-groove preparations are more costly to prepare because they typically involve machining or air-arc gouging. The curved surface details usually require less weld metal in order to obtain a weld of the same strength as the planar surface alternatives.
When properly detailed and welded, any of the CJP groove weld details will yield a connection equal in strength to the connected material. Similarly, a variety of PJP groove weld details can be used to achieve the specified effective throat dimensions. As a result, the typical practice in the structural steel industry is for the engineer to leave the selection of the groove weld type and details up to the contractor. Based upon factors such as knowledge and experience, the plan of fabrication and erection, as well as available equipment, the contractor selects the groove weld detail that yields the required quality at the lowest cost.
Source: AISC Design Guide 21

## Slide 83: Weld TYPES
Complete joint penetration (CJP) groove weld
Partial joint penetration (PJP) groove weld
Notes: By definition, complete joint penetration (CJP) groove welds have a throat dimension equal to the thickness of the plates that they join. In the past, these welds were known as complete penetration (CP) welds, and before that, full penetration (FP) welds. For statically loaded structures, CJP groove welds develop the full strength of the attached materials.
CJP groove welds may be applied to butt, T-, and corner joints. They are often required in butt joints loaded in tension. When butt joints are loaded in compression, and for T and corner joints loaded in shear, design requirements rarely justify the use of CJP groove welds. In general, the prequalified CJP groove weld details listed in AWS D1.1 require steel backing if made from one side and back gouging if made from both sides.
This ensures complete fusion throughout the thickness of the material being joined. In general, for CJP groove weld details welded from one side without steel backing, or for two sided details without backgouging, procedure qualification testing is required to prove that the full throat is developed.
A special exception to this is applied to tubular connections, for which CJP groove welds may be made from one side without backing.
CJP groove welds have two advantages over other weld types, and these advantages have also resulted in widespread abuse with respect to the tendency to specify CJPs in situations where there are better options. As has been mentioned, these welds develop the full strength of the connected material.
Thus, one advantage of these welds is that no design calculations are required when CJP groove welds are used in statically loaded structures. The simple specification of “CJP” in the tail of the welding symbol is sufficient to ensure that when fabricated according to the applicable standards, the weld will develop the strength of the connected material.
A PJP groove weld is one that, by definition, has a throat dimension less than the thickness of the materials it joins. PJP groove welds can be applied to butt, corner, and T-joints. They are commonly used for column splices where the butt joint is usually loaded in compression, or with only limited tension. PJP groove welds are also commonly used in corner joints of built-up box columns. Both
fillet welds and PJP groove welds can be used in T-joints, and inside corner joints. The relative economic advantages of both are discussed in Section 14.2 of this Design Guide 21.
Source: AISC Design Guide 21

## Slide 84: Weld Types
Weld Terminology
Notes: Of primary interest to the designer is the dimension noted as the “throat.” The throat is theoretically the weakest plane in the weld and therefore controls the design of many welds.
Source: AISC Design Guide 21

## Slide 85: Weld Types
Fillet Weld Terminology
Notes: Fillet welds have a triangular cross-section and are applied to the surface or edges of the materials that they join. Fillet welds by themselves do not fully fuse the cross-sectional areas of parts that they join, although it is usually possible to develop full-strength connections with fillet welds alone. Fillet welds can be applied to T- and lap joints, and to the inside corner of corner joints. Fillet welds may be used to add strength to PJP groove welds, and may be used to provide for a more gradual contour to CJP groove welds in T- and corner joints. When used in conjunction with CJP groove welds, the strength of the fillet weld is not added to that of the CJP groove weld.
Fillet welds are used extensively in structural steel fabrication and are often used to join shear tabs to columns, gussets to beams and columns, stiffeners to webs, and light columns to base plates, as well as many other examples.
The size of a fillet weld is specified in terms of the leg size, even though the strength of the weld is theoretically controlled by the throat size. For equal-legged, flat-faced, or convex-faced fillet welds applied to surfaces that are oriented 90° apart, the throat dimension is found by multiplying the leg size by 0.707 (e.g., sin 45°).
Because fillet welds do not fuse the cross-section of the joint, there will always be an unfused plane under the root of the fillet, or in the case of double-sided fillets, between the two (unless the fillet is applied on top of a groove weld).
Source: AISC Design Guide 21

## Slide 86: Weld Types
FEXX = filler metal classification strength, ksi
This is also known as the minimum specified tensile strength of the weld electrode (i.e. 60, 70, 80, 90, 100, 110 or 120 ksi)
E70XX (FEXX = 70 ksi) is considered matching for 36 and 50 ksi (Fy) base metals so it is the most common electrode in structural welds

## Slide 87: Weld Dimensional Limitations
Effective Areas (J2.1a)
The effective length, Lweld , multiplied by the effective throat, teff
Aw = teff x Lweld
teff= 0.707t
Toe
Toe
Base Metal
Base Metal
teff
t
t
Notes: The effective area of a fillet weld shall be the effective length multiplied by the effective throat. The effective throat of a fillet weld shall be the shortest distance from the root to the face of the diagrammatic weld. An increase in effective throat is permitted if consistent penetration beyond the root of the diagrammatic weld is demonstrated by tests using the production process and procedure variables.
For fillet welds in holes and slots, the effective length shall be the length of the centerline of the weld along the center of the plane through the throat. In the case of overlapping fillets, the effective area shall not exceed the nominal cross-sectional area of the hole or slot, in the plane of the faying surface
Source: AISC 360-16, Chapter J

## Slide 88: Weld dimensional Limitations
Notes: This minimum size has nothing to do with design but is specified for practicality. Concern is also for welding heat input/cracking resistance.
The minimum weld sizes in Table J2.4 of AISC 360-16 are not design related requirements but are used to address welding-related concerns that involve fusion and cracking. In order to make a good arc weld, there is a minimum amount of thermal energy that must be introduced into the joint. Failure to do so may result in the deposition of weld metal, albeit without fusion to the base metal. Alternatively, when insufficient thermal energy is delivered to the joint, the cooling rate experienced by the weld and the heat-affected zone may be such that cracking occurs. To ensure that a reasonable level of thermal energy is introduced into the joint, AISC Specification Table J2.4 requires that a certain minimum weld size be applied, regardless of design loads. This is possible because there is a direct relationship between the thermal energy introduced into the joint and the weld size applied to the joint. This assumes, however, that the weld size is applied in a single pass.
The minimum fillet weld size need never exceed the thickness of the thinner part being joined. In some extreme circumstances, the connection might involve an extremely thick plate being joined to a very thin plate. The AISC Specification dictates that the weld need not exceed the size of the thinner part. However, under these circumstances, additional preheat based on the thicker material may be justified.
Source: AISC Design Guide 21

## Slide 89: Weld dimensional limitations
Maximum Fillet Weld Sizes (J2.2b(a) and (b))
Depends on the thickness of the connecting parts:
Notes: Both the AISC Specification and AWS D1.1 have provisions that specify maximum fillet weld sizes. These provisions are frequently misunderstood and misapplied. AISC Specification Section J2.2b requires a maximum fillet weld size along the edges of material 1/4 in. or more in thickness. Note that this applies only to the situation where welds are applied “along the edges.” Such conditions include lap joints, and some corner joint configurations, but do not include T-joints. These provisions came about because it is possible for welders (particularly when using SMAW electrodes) to melt away the top edge of the member when welding on an edge.
This creates a weld with a normal weld toe dimension, but the corresponding weld throat may be much smaller than the designer intended. Melting away the top edge is not detrimental to the welded joint, provided that the required throat dimension is obtained. For thinner materials (identified as less than 1/4 in. thick), this situation is less likely to occur, and thus these provisions only apply to the edges of thicker members.
If it is required for a weld to have more capacity than is provided with a fillet weld with a leg size that is 1/16 in. less than the thickness of the edge, it may be possible to specify an unequal legged fillet, allowing the other leg to be larger.
Source: AISC Design Guide 21

## Slide 90: Weld dimensional limitations
Maximum Fillet Weld Sizes (J2.2b(a) and (b))
Only applies to welds along edges (i.e., not T-joints)
Notes: The provisions of Section J2.2b apply only to situations where welds are applied “along the edges” such as lap joints (shown), and some corner configurations. This does not include T-joints.
The common misuse of the provisions of Section J2.2b comes about when they are applied to situations involving the placement of welds on a surface versus on an edge. Consider a tube column welded to a base plate. A fillet weld may be specified, and may be required to develop the full capacity of the tube wall. Assuming access to the inside of the tube is limited (as is typically the case), the single-sided weld will often need to have a leg size that exceeds the tube wall thickness. The maximum fillet weld size provisions do not apply in this situation since the weld is not on an edge.
Source: AISC Design Guide 21
Sidenote: For T and Corner joints, there is no maximum fillet weld size. BUT any time a weld is bigger than the connected part thickness, the designer has to think about both the strength of those connected parts and how those parts will perform during the life of the structure. (Thus, it’s usually better not to use a weld bigger than the connected part thickness)

## Slide 91: Weld dimensional limitations
Notes: For thicker members in lap joints, it is possible for the welder to melt away the upper corner, resulting in a weld that appears to be full size but actually lacks the required weld throat dimension. See Figure C-J2.1(a). On thinner members, the full weld throat is likely to be achieved, even if the edge is melted away. Accordingly, when the plate is 1/4 in. (6 mm) or thicker, the maximum fillet weld size is 1 /16 in. (2 mm) less than the plate thickness, t, which is sufficient to ensure that the edge remains.
Source: AISC 360-16 Chapter J Commentary

## Slide 92: Weld Dimensional limitations
Minimum Weld Length (J2.2b(c))
or
Size of weld shall not be taken to exceed one-quarter of its length
Notes: AISC Specification Section J2.2b requires that fillet weld lengths be at least four times the leg size. For welds that do not meet this criterion, the effective weld size is to be taken as 4 of its length. The four times length provision, combined with the Table J2.4 minimum fillet weld size, results in a minimum weld length requirements as a function of the thickness of the material being joined, although such provisions are not explicitly stated.
Source: AISC Design Guide 21

## Slide 93: Weld Dimensional limitations
End-Loaded Fillet Welds – Effective Length (J2.2b(d))
For end-loaded fillet welds with a length up to 100 times the weld size, it is permitted to take the effective length equal to the actual length.
When the length of the weld exceeds 300 times the leg size, w, the effective length shall be taken as 180w.
Notes: When longitudinal fillet welds parallel to the stress are used to transmit the load to the end of an axially loaded member, the welds are termed “end loaded.” Typical examples of such welds include, but are not limited to (a) longitudinally welded lap joints at the end of axially loaded members, (b) welds attaching bearing stiffeners, and (c) similar cases. Typical examples of longitudinally loaded fillet welds that are not considered end loaded include, but are not limited to (a) welds that connect plates or shapes to form built-up cross sections in which the shear force is applied to each increment of length of weld depending upon the distribution of the shear along the length of the member, and (b) welds attaching beam web connection angles and shear plates because the flow of shear force from the beam or girder web to the weld is essentially uniform throughout the weld length; that is, the weld is not end-loaded despite the fact that it is loaded parallel to the weld axis. Neither does the reduction coefficient, β, apply to welds attaching stiffeners to webs because the stiffeners and welds are not subject to calculated axial stress but merely serve to keep the web flat.
Source: AISC 360-16, Chapter J Commentary

## Slide 94: Weld Dimensional limitations
End-loaded Connection
Weld subject to shear loading due to bending forces
NOT end-loaded
End-Loaded Fillet Welds
Notes: “End loaded” applies to connections where the load is transferred to the end of a weld. The left figure on this slide illustrates one such example. Many lap joints with longitudinal welds have end-loaded fillet welds, as do bearing stiffeners.
Welds subject to shear loading due to bending forces, such as those shown in the right figure, are not included in end-loaded applications. In addition, transversely loaded welds are not considered end loaded.
The distribution of stress at the end of welds, such as the one shown in the left image is far from uniform. The relative stiffness of the weld versus the two lapped members might be significantly different. Shear lag further complicates the stress distribution. Due to these factors, and perhaps others as well, the full length of the weld might not be uniformly loaded. At some length, it becomes unconservative to assume the length of the weld is equally effective in transferring stress. That is why the effective length exists.
Based on experience and research, a ratio of the weld leg size to weld length has been determined to be a critical factor in determining the effective length. When this ratio is 100 or less, the entire length can be considered effective. Thus, ¼” (6 mm) welds less than 25” (600 mm) long, and 3/8” (10 mm) welds less than 37.5” (1000 mm) long are no problem and can be treated in the conventional manner. Therefore, for many applications, concern about welds that are “too long” will not occur.
Source: “Fillet Welds that are “too long”” – Duane Miller (https://www.aisc.org/globalassets/modern-steel/archives/2003/03/2003v03_fillet.pdf)

## Slide 95: Weld Dimensional limitations
End-Loaded Fillet Welds – Effective Length (J2.2b(d))
When the length of the end-loaded fillet weld exceeds 100 times the weld size, the effective length shall be determined by multiplying the actual length by the reduction factor, β, determined as:
β = 1.2 − 0.002(l /w) ≤ 1.0 (J2-1)
where l = actual length of end-loaded weld
w = size of weld leg
Notes: The Specification provides a β (beta) reduction factor to adjust the actual length to obtain the effective length. The effective length is the length of weld effective in transferring stress.
For reference, the effective length applies with an actual length of 32 inches for a 5/16 fillet weld.

## Slide 96: Weld Dimensional limitations
End-Loaded Fillet Welds – Effective Length (J2.2b(d))
Notes: This chart of effective length vs actual length will be included in the AISC 360-22 Spec.
Up until 100 times the weld size (w), the effective length and actual length are the same. This linear relationship changes for effective lengths beyond 100w.
The Spec states (and is reflected in this chart) that when the actual length of the weld exceeds 300 times the weld size (w), the effective length shall be taken as 180w.

## Slide 97: Weld Dimensional limitations
Intermittent Fillet Welds (J2.2b(e))
Intermittent fillet welds are permitted to be used to transfer calculated stress across a joint or faying surfaces and to join components of built-up members.
The length of any segment of intermittent fillet welding shall be not less than four times the weld size, with a minimum of 1 1/2 in.

## Slide 98: Weld symbols
AWS A2.4-20 (Figure 4.3)
Notes: The image in this slide is from AWS D1.1 and AWS A2.4-20. (D = depth, S = size)
In the 15th Edition of the Steel Manual (Chapter 8), “S(E)” was used instead of “S or D(S)”, where S = size, E = effective throat. It is expected that the table shown on this slide will be reflected in the 16th Edition of the Steel Manual.

## Slide 99: Weld Symbols
AWS A2.4-20 (Figure 4.1)
Notes: Table 8-2 in the 15th Edition of the Steel Manual has a similar table.

## Slide 100: Weld Symbols
AWS A2.4-20 (Figure 4.2)
Notes: Table 8-2 in the 15th Edition of the Steel Manual has a similar table.

## Slide 101: Weld symbols – Fillet Welds
Indicates fillet weld on:
Other side of connecting material
Arrow side of connecting material
Notes: The location of the symbol above and/or below the horizontal line indicates whether the weld is on the arrow side of the connection material (below) or the other side of the connecting material.
The figures show how the symbol location and arrows indicate where the welds should occur.
Also note that no matter whether the arrow comes from the left or right side of the horizontal line, the information and symbol is always oriented the same way from left to right: size, then symbol, then length. It does not change with a change in direction arrow.

## Slide 102: Weld symbols – Fillet Welds
1/4
14
This results in a 1/4” thick weld that is 14” long on the side of the arrow
14”

## Slide 103: Weld symbols – Fillet Welds
1/4
2-4
This results in ¼” intermittent welds that that are 2” long spaced at 4”
2”
4”
Notes: If long segments of weld are not required, intermittent welds can be used. 2-4 indicates 2” long at a 4” spacing.

## Slide 104: Weld symbols – CJP Welds
Complete joint penetration (CJP) groove weld
Indicates V weld on:
Other side of connecting material
Arrow side of connecting material
Notes: CJPs are complete joint welds that can be achieved through various types of welding including V, bevel, U, flare V, flare bevel, etc.
Generally the designer will specify CJP and may or may not dictate the particular type of CJP weld to be made. Here the V weld on either side is used, as is shown by the V symbol above and below the horizontal line.

## Slide 105: Weld symbols – CJP Welds
Indicates bevel weld
Indicates root opening
Indicates groove angle
backing bar
Indicates backing bar
1/8
45o
45o
1/8”
Notes: This image shows a full depth bevel. The additional information of the root opening and groove angle are typically dictated by the fabricator, not the structural designer.

## Slide 106: Weld symbols – PJP Welds
Partial joint penetration (PJP) groove weld
Indicates U weld
3/4
3/4”
60o
Indicates groove angle
Indicates weld size
60o
Notes: Like CJPs, there are a number of PJP options for welding. Here is just one example showing a partial depth U weld.