## Slide 1: Design and analysis of Steel Connection Types
Prepared by: Dr. Rachel Chicchi , University of Cincinnati
with the support of the American Institute of Steel Construction
3. Constructability Considerations
Version 1 – January 2022
Notes: This series of PowerPoint presentations covers the fundamentals of the design and analysis of steel connections. The intention of these slides was to focus on simple (shear) connections and include all aspects of connection design and detailing, including design procedures and constructability considerations. Given the volume of the content, basic fundamentals were provided which do not dig in closely to the design portion of the connections. If you would like slides related to specifics of shear connection design, you may reach out to Rachel Chicchi to obtain these additional slides.
The material can be used at the graduate or undergraduate level. Portions can also be used for construction management or architecture students.
This module is #3 – Constructability Considerations
For questions, comments, corrections, or suggestions on these presentations, please contact:
Rachel Chicchi
Civil & Architectural Engineering and Construction Management
University of Cincinnati
2850 Campus Way Drive
765 Baldwin Hall
Cincinnati, OH 45221
Email: rachel.chicchi@uc.edu
Acknowledgments:
These presentations were prepared with support from the AISC Teaching Aid Development Program. Overall coordination of this effort was provided by Kristi Sattler at AISC. The author gratefully acknowledges support provided by AISC and the coordination and oversight provided by Dr. Sattler.
The author also gratefully acknowledges contributions and review provided by the AISC review committee for this project:
Hans Herrmann – Mississippi State University
Jason McCormick – University of Michigan
Tim Mrozowski – Michigan State University
Other contributions to add:
Judy?
Jim / GA?
Others reviewing the work?

## Slide 2: Design and analysis of steel connections
1 - Introduction, Basic Principles, and Limit States
2 - Connection Basics: Bolts & Welds
3 - Constructability Considerations
Notes: This PowerPoint series is divided into 3 modules. This is the third module on “Constructability Considerations”
Note that there were 3 other modules previously planned. Refer to the ReadMe for information on these modules and feel free to contact the author with requests for these additional files.

## Slide 3: Steel Connections & Safety
Steel connections are a combination of structural elements and joints used to transmit forces between two or more members.
Connections are critical to ensuring proper load path in a structural system, and ductility is essential to successful connections.
Connections allow individual members (that can be easily fabricated, transported, and erected) to be connected to other members in order to create the structural frame.

## Slide 4: Steel Connections & Safety
Connections are critical to ensuring proper load path in a structural system.
Thus, safety is paramount for all phase of connection design, fabrication, and erection.
Connection integrity must be maintained during erection and proper installation and inspection procedures must be followed.

## Slide 5: Steel Connections
Primary method of connecting elements are:
Bolting
Welding
Notes: Bolts and welds are the primary methods for connecting structural steel elements. These two methods are covered in more detail in Module 2.

## Slide 6: Shop vs Field Connections
Connection designer must consider constructability. These decisions also play a large role in connection costs.
The choice between bolting and welding is complex and depends on geometry of the connection, properties of the connected members, available equipment, and qualified labor, among other factors.
Quality welded and bolted connections can be achieved in both the shop and the field.
Notes: It is unlikely that there are any operations (drilling, bolting, sandblasting, painting, etc.) that are more economically done in the field versus in the shop, and welding is no different.
The practical implementation of this principle is simply to specify welding in the shop to the greatest extent possible. Whenever possible, large or complicated connections should be welded in the shop, leaving the simpler connections for field welding. In rare situations, this may even justify the creation of an additional splice, as is done with tree-column connections; at the node, complicated connections are made in the shop, and at the ends of the tree branches, simpler splices are made in the field. Regardless of where welding is performed, it must be done in a safe manner, and the resulting weld must meet the quality requirements. Field conditions are more demanding, but both safety and quality can be achieved in the field when the site is properly supervised and managed.
Source: AISC Design Guide 21

## Slide 7: 3 - Constructability considerations
Erection & Safety
Bolt Inspection
Weld Safety & Inspection
Base Plate Connections
Splices
Tolerances
Best Practices for Connections
Notes: These topics will be explained in more detail throughout this lecture.

## Slide 8: Erection & Safety
Steel is fabricated off-site as individual members and erected together with steel connections on-site
Notes: You can see columns here which have already been fabricated. The holes on the left side are for bolted column splice connections.

## Slide 9: Erection & Safety
The erector is required to maintain structural stability at all times during the erection process.
This includes using the necessary number of bolts required to temporarily support members.
Notes: The engineer needs to tell the contractor when and where the structure may need additional bracing beyond the frame steel for stability. The engineer has to identify the lateral system. The erector is responsible for maintaining stability at all times during erection and selecting an erection sequence that ensures stability.

## Slide 10: Erection & Safety
Typical sequence of a multi-story steel building:
- Erect two-story columns
- Erect floor framing
- Spread upper deck as lower deck is spread
- Install next tier of columns
- Plumb
- Finish bolting and welding connections
- Connect the deck

## Slide 11: Erection & Safety

## Slide 12: Erection & Safety

## Slide 13: Erection & Safety
Minimum Erection Bolts
Two bolts in each connection are minimum to connect solid web members during erection
One bolt in each connection for bracing members during erection
Notes: Provides structural integrity during erection while also allowing some movement for plumbing
Per OSHA 1926 Subpart R: 1926.756(a)(1) : During the final placing of solid web structural members, the load shall not be released from the hoisting line until the members are secured with at least two bolts per connection, of the same size and strength as shown in the erection drawings, drawn up wrench-tight or the equivalent as specified by the project structural engineer of record, except as specified in paragraph (b) of this section.
1926.756(b)Diagonal bracing. Solid web structural members used as diagonal bracing shall be secured by at least one bolt per connection drawn up wrench-tight or the equivalent as specified by the project structural engineer of record.
Plumbing will be easier if bolts are not all fully installed.
Note: Bridge girder are often required to have half of their bolts installed before they are cut loose. And they may have pins in other holes.

## Slide 14: Erection & Safety
Recommended Connection Length
The minimum length of connection should be at least ½ of the T-dimension of the supported beam.
This provides beam end stability during erection
Connection length
T

## Slide 15: Erection & Safety
Recommended Connection Length
Connecting elements (i.e. – plate or angle) must be compatible with T-dimension with minimal encroachment
Notes: Figure 10-3 is taken from the AISC Steel Construction Manual, 15th Edition.

## Slide 16: Erection & Safety
One vs Two-sided Connections
Two-sided shear connections (such as double-angle and end- plate) must be considered carefully during erection to ensure a continuous load path
One-sided
Two-sided
Notes: The Manual (Part 10) takes time to note the difference between one-sided and two-sided connections. Examples of each are shown in this slide.

## Slide 17: Erection & Safety
One vs Two-sided Connections
One-sided connections have the following advantages:
- Shop attachment of connection elements to the support, simplifying shop fabrication and erection
- Reduced material and shop labor requirements
- Ample erection clearance is provided
- Excellent safety during erection since double connections often can be eliminated
Notes: One-sided connections are advantageous for the reasons listed above.
The two-sided connections (double-angles and end-plates) have clearance issues that are not as prevalent in one-sided connections.

## Slide 18: Erection & Safety
One vs Two-sided Connections
Two-sided connections have the following advantages:
- Can be used when the end reaction is large (more bolts and/or double shear)
- Compact connections (usually the entire connection is contained within the flanges of the supported beam)
- Eccentricity perpendicular to the beam axis need not be considered for workable gages (the connection is symmetric perpendicular to the beam)

## Slide 19: Erection & Safety
Two-sided Connection Concerns
brought into its final position
Positive connection must be made and maintained for the first member to be erected while the second member is erected.
Notes: Figure 10-2 comes from the AISC Steel Construction Manual and shows use of a temporary erection seat for the first beam while the second beam is erected.
OSHA 1926.756(c)(1)Double connections at columns and/or at beam webs over a column. When two structural members on opposite sides of a column web, or a beam web over a column, are connected sharing common connection holes, at least one bolt with its wrench-tight nut shall remain connected to the first member unless a shop-attached or field-attached seat or equivalent connection device is supplied with the member to secure the first member and prevent the column from being displaced (See Appendix H to this subpart for examples of equivalent connection devices).
1926.756(c)(2)If a seat or equivalent device is used, the seat (or device) shall be designed to support the load during the double connection process. It shall be adequately bolted or welded to both a supporting member and the first member before the nuts on the shared bolts are removed to make the double connection.

## Slide 20
Positive connection can be achieved by staggering angles or using an erection seat
Notes: Example of beam with angles staggered and shop-welded to the beam.

## Slide 21
Bolt stagger
Notes: This image shows staggering of bolts for double-angle connection framing into column web. You can see that the beam framing in on the other side (out of view) has its top bolt above the top bolt of the close beam.

## Slide 22: Erection & Safety
Two-sided Connections
Also a problem framing into girders:
Members must be secured with at least two bolts per connection before removing hoisting line
In order to bolt in the second beam, the first beam would need to be temporarily braced and bolts removed
Notes: Section 1926.756(a)(1) states: “During the final placing of solid web structural members, the load shall not be released from the hoisting line until the members are secured with at least two bolts per connection.” The issue with this connection is that an ironworker will need to temporarily support the first beam without bolts (or remove the bolts from the first beam that is connected) in order to connect the second beam. Yet the first beam cannot be released from the hoisting line until it has two bolts in each connection that cannot subsequently be removed to permit erection of the second beam, per OSHA requirement. There are many solutions available, and all eliminate the sharing of all bolts in a common field connection.
Source: AISC Steel Quiz Febr 2015

## Slide 23: Erection & Safety
When beams frame opposite each other but slightly offset, connection can be designed with all bolts on the same gage lines
Bolts shared;
in double shear and carry additional load
Notes: This is the first part of Figure 10-26 (continued on next slide). It comes from the AISC Steel Construction Manual.
When beams frame opposite each other and are welded to the web of the supporting girder or column, there are usually no dimensional constraints imposed on one connection by the presence of the other connections unless erection bolts are common to each connection. When the connections are bolted to the web of the supporting column or girder, however, the close proximity of the connections requires that some of all fasteners be common to both connections. This is known as a double connection.
When beams of different nominal depths frame into a double connection, care must be taken to avoid interference from the bottom flange of the shallower beam with the entering and tightening clearances for the bolts of the connection for the deeper beam. Access to the bolts that will support the deeper beam may be provided by coping or blocking the bottom flange of the shallower beam. Alternatively, stagger may be used to favorably position the bolts around the bottom flange of the shallower beam.
Frequently, beams do not frame exactly opposite each other but are slightly offset, as illustrated in Fig 10-26. Several connection configurations are possible, depending on the offset dimension.
If the offset were equal to the gage on the support, the connection could be designed with all bolts on the same gage lines, as shown in Figure 10-26 (b) , and the angles arranged as shown in Fig 10-26 (d). If the offset were less than the gage on the support, staggering the bolts, as shown in Fig 10-26(c), would reduce the required gage and the angles could be arranged, as shown in Fig 10-26(c). In any case, each bolt transmits an equal share of its beam reaction(s) to the supporting member, with the bolts that are loaded in double shear ultimately carrying twice as much force as those loaded in single shear. Once the geometry of the connection has been determined, the distribution of the forces is patterned after that in the design of a typical connection. For normal gages, eccentricity may be ignored in this type of connect.
Source: AISC Steel Construction Manual, 15th Edition

## Slide 24: Erection & Safety
Or connection can be designed with bolts staggered
Bolts staggered
Bolts shared; in double shear and carry equal load
Notes: See previous slide for discussion.

## Slide 25: Erection & Safety
Temporary Bracing
Notes: Temporary bracing is used to ensure stability until all of the framing and connections are secured during erection.
The cables shown may be installed for two reasons: plumbing and stability. Plumbing cables will not assure stability unless they are designed for that purpose
AISC Code of Standard Practice:
Many structural steel frames have lateral force-resisting systems that are activated during the erection process. Such lateral force-resisting systems may consist of welded moment frames, braced frames or, in some instances, columns that cantilever from fixed-base foundations. Such frames are normally braced with temporary guys that, together with the steel deck floor and roof diaphragms or other diaphragm bracing that may be included as part of the design, provide stability during the erection process. The guy cables are also commonly used to plumb the structural steel frame. The erector normally furnishes and installs the required temporary supports and bracing to secure the bare structural steel frame, or portion thereof, during the erection process. When erection bracing drawings are required in the contract documents, those drawings show this information

## Slide 26: Erection & safety
Plumbing of the Structure
Vertical alignment of the structure
Erector is responsible for installation of framing to the specified plumbness, elevation & alignment within erection tolerances (per AISC Code of Standard Practice)
Generally, maximum permitted out-of-plumb:
Δ = L/500
L
Plumb Structure
Out-of-Plumb Structure
Δ
L
Notes: AISC Code of Standard Practice: Columns with attached base plates, beams with attached bearing plates and other similar members with attached bearing devices that are temporarily supported on leveling nuts and washers, shims or other similar leveling devices, shall be promptly grouted after the structural steel frame or portion thereof has been plumbed.
Permissible angular variation of column work lines are given with respect to a plumb line which is generally 1/500 of the distance between working points.

## Slide 27: Erection & Safety
Notes: Guy cables in the temporary bracing is typically used to plumb the structural steel frame.

## Slide 28: Erection & Safety
Notes: These cables can be adjusted in length as necessary to pull the structure to plumb.

## Slide 29: Erection & Safety
Bolt Tightening
After the structure has been plumbed, connections should all be secured (all bolts and in-field welds installed) prior to removing temporary bracing.
At no time shall there be more than four floors or 48 feet of unfinished bolting or welding above foundation or permanently secured floor.
Ensure bolts reach necessary pretension if specified (check twist offs, DTIs, etc.). Use snug-tight wherever possible.
Notes: At no time shall there be more than four floors or 48 feet (14.6 m), whichever is less, of unfinished bolting or welding above the foundation or uppermost permanently secured floor, except where the structural integrity is maintained as a result of the design.
Source: OSHA – 1926.754(b)(2)

## Slide 30: Bolt tightening
Notes: This photo shows the bolts prior to tightening. You can see gaps between the plies (the angle and the column web).

## Slide 31: Bolt tightening
Notes: As mentioned in Module 2, there are a number of methods for bolt tightening including a standard wrench and impact wrench.

## Slide 32: Erection & Safety
Bolt Tightening
Connection details must provide proper clearance to install and tighten the bolts
Use common gages for angles, T-shapes and W-shapes, etc.
Workable gage is the spacing for fasteners in the flange that provides for entering and tightening clearances and edge distance and spacing requirements
Tight conditions or skewed connections may eliminate some bolt tightening methods from being possible

## Slide 33
Notes: Table 1-7A gives workable gages based on different angle legs.
Table 7-15 shows the entering and tightening clearances needed for A325 and A490 bolts. The table includes other types of bolts as well.
Both of these tables can be found in the AISC Steel Construction Manual.

## Slide 34
Notes: Table 1-1 shows dimensional properties for the W-shape including the workable gage. This is the transverse spacing of the bolts in the flange that provides for entering and tightening clearances and edge distance and spacing requirements.
Using the workable gages from Table 1–1 is always suggested to help standardize details and simplify coordination, for example between the joist supplier and the steel fabricator. However, there may be cases when other gages are needed for more efficient connections. For example:
Four bolts across the flange (of course, when the flange is wide enough) in a bolted flange-plated moment connection makes the connection more compact;
Smaller gages may be required for hanger connections to eliminate reinforcement for flange bending
Source: https://www.aisc.org/globalassets/modern-steel/archives/2010/05/2010v05_workable_flange_gages.pdf)

## Slide 35: Erection & Safety
.
Additional Options to Ensure Bolt Tightening Clearance
Stagger shop & field bolts to provide ample clearance as shown
Staggering bolts is also beneficial for erection safety & stability
Manual Table 7-15 can be used to check clearances

## Slide 36: Erection & Safety
.
Additional Options to Ensure Bolt Tightening Clearance
Increase connection angle gages to provide adequate driving clearance
Section A

## Slide 37: 3 - Constructability considerations
Erection & Safety
Bolt Inspection
Weld Safety & Inspection
Base Plate Connections
Splices
Tolerances
Best Practices for Connections

## Slide 38: Bolt inspection
The most important features in the inspection of installation of high-strength bolts are:
• To know whether bolt pretension is required or not. If bolt pretension is not required, do not inspect for it.
• To know what pre-installation verification is required and to monitor it at the job site on a regular basis.
• To observe the work in progress on a regular basis.
Notes: See slides in Module 2 which discusses pretensioning of bolts.
Pretensioned bolts are used where the bolts are required to be fully tensioned but the slip resistance is not relied upon to transfer load. Appropriate when pretension is desired for reasons other than slip resistance. Pretensioned joints have some additional installation costs over snug-tightened joints.
Common applications of pretensioned joints are:
  Joints in which fastener pretension are required in the Specification;
  Joints that are subject to significant load reversal;
  Joints that are subject to fatigue load with no reversal of the loading direction;
  Joints with Group 120 bolting assemblies that are subject to tensile fatigue;
  Joints with Group 144 or Group 150 bolting assemblies that are subject to tension or combined shear and tension, with or without fatigue.

## Slide 39: Bolt inspection
For snug-tight joints:
• Establish that bolts, nuts, washers (if required) and condition of faying surfaces meet the RCSC Spec requirements
• Verify hole types and bolt grades conform with the drawings
• Ensure faying surfaces are free of loose scale, dirt, etc.
• Verify steel parts fit solidly together
Notes: For those joints where the bolts need only to be brought to the snug-tight condition, inspection is simple and straightforward. There is no verification procedure associated with snug-tightened bolt installation. The inspector should establish that the bolts, nuts, washers (if required), and the condition of the faying surfaces of the parts to be connected meet the RCSC Specification requirements. Hole types (e.g., oversize, slotted, normal) shall be in conformance with the contract documents. The faying surfaces shall be free of loose scale, dirt, or other foreign material. Burrs extending up to 1/16 in. above the plate surface are permitted. The inspector should verify that all material within the grip of the bolts is steel and that the steel parts fit solidly together after the bolts have been snug-tightened. The contact between the parts need not be continuous. These requirements apply equally to A325 and A490 high-strength bolts and to A307 ordinary bolts.
Source: AISC Design Guide 17

## Slide 40: Bolt inspection
For pretensioned joints (in addition to inspection process for snug-tight):
• Verification process must be employed and pre-installation testing must be observed
• Testing consists of installation of representative number of fasteners in a device capable of indicating bolt pretension (i.e. – calibrated wrench, calibrating tension- control bolts, etc.)
Notes: Calibrated wrenches and TC bolts are explained further in Module 2, including photos.
If the designer has determined that pretensioned bolts are required, then the inspection process becomes somewhat more elaborate than that required for snug-tightened bolts.
In addition to the requirements already described for snug-tightened bolts, the principal feature now is that a verification process must be employed and that the inspector observe this pre-installation testing. For any method selected, this testing consists of the installation of a representative number of fasteners in a device capable of indicating bolt pretension. (See Section 3.2.2 in the AISC Design Guide 17 for a description of this process.) The inspector must ensure that this is carried out at the job site and, in the case of calibrated wrench installation, it must be done at least daily. If any conditions change, then the pre-installation testing must be repeated for the new situation.
Source: AISC Design Guide 17

## Slide 41: Bolt inspection
For pretensioned joints (in addition to inspection process explained for snug-tight):
• For tension control (TC) bolts, look for splined tips that haven’t sheared off (routine observation of installation to ensure being done correctly)
• For turn-of-nut, routine observation of crew or matchmarking can be used
• For DTIs, determine that washer configuration is appropriate and feeler gage is refused in at least half of the openings
Notes: The inspector must ensure that this is carried out at the job site and, in the case of calibrated wrench installation, it must be done at least daily. If any conditions change, then the pre-installation testing must be repeated for the new situation. For example, if the initial calibration of tension-control bolts was done for 4 in. long 3/4 in. diameter A325 bolts but 6 in. long 3/4 in. diameter bolts of the same grade must also be installed on the same day, then a second calibration is required.
In the case of turn-of-nut pretensioning, routine observation that the bolting crew applies the proper rotation is sufficient inspection. Alternatively, matchmarking can be used to monitor the rotation. Likewise, if calibrated wrench installation has been used, then routine observation of the field process is sufficient. Because this method is dependent upon friction conditions, limits on the time between removal from storage and final pretensioning of the bolts must be established.
Inspection of the installation of twist-off bolts is also by routine inspection. Since pretensioning of these bolts is by application of torque, a time limit between removal of bolts, nuts and washers and their installation is required, as was the case with calibrated wrench installation. Observation that a splined tip has sheared off is not sufficient evidence in itself that proper pretension exists, however. This only signifies that a torque sufficient to shear the tip was present in the installation history. It is important that twist-off bolts first be able to sustain twisting without shearing during the snugging operation. It is therefore important that the inspector observe the preinstallation
of fastener assemblies and assess their ability to compact the joint without twist-off of tips.
For direct-tension indicator pretensioning, routine observation can be used to determine that the washer protrusions are oriented correctly and that the appropriate feeler gage is accepted in at least half of the spaces between protrusions. After pretensioning, routine observation can be used to establish that the appropriate feeler gage is refused in at least half the openings. As was the case for twist-off bolts, simply establishing that the indictor washer gaps have closed can be misleading. The snug-tightening procedure must not produce closures in one-half or more of the gaps that are 0.015 in. or less.
The RCSC Specification provides a method of arbitration for bolts that have been installed and inspected according to one of the approved methods, but where disagreement has arisen as to the actual pretension in the installed bolts. A manual torque wrench is used to establish an arbitration torque that can then be applied to the bolts in question. As is pointed out in the Commentary to the RCSC Specification, such a procedure is subject to all of the uncertainties of torque-controlled calibrated wrench installation. In addition, other elements necessary to control the torque-related issues may be absent. For example, an installation done originally by turn-of-nut with no washers will be influenced by this absence of washers when the arbitration inspection is applied.
Source: AISC Design Guide 17

## Slide 42: 3 - Constructability considerations
Erection & Safety
Bolt Inspection
Weld Safety & Inspection
Base Plate Connections
Splices
Tolerances
Best Practices for Connections

## Slide 43: Weld Safety
Welding is a safe operation when sufficient measures are taken to protect welder from potential hazards such as: electrical shock, overexposure to arc radiation, fumes and gases, and fire and explosions.
Safety Resources:
ANSI Z49.1:2012 - Safety in Welding, Cutting, & Allied Processes *
AWS Safety & Health Fact Sheets *
Manufacturers’ material safety data sheets (MSDSs) for welding equipment and consumables
* available as a free download from (http://www.aws.org/)
Notes: Welding is a safe operation when sufficient measures are taken to protect the welder from potential hazards. When these measures are overlooked or ignored, welders can encounter such dangers as electrical shock; overexposure to arc radiation, fumes, and gases; and fire and explosions—any of which may result in fatal injuries. ANSI Z49.1:2005, Safety in Welding, Cutting, and Allied Processes, available as a free download from AWS (http://www.aws.org/), should be consulted for information on welding safety.
From the same site, a variety of AWS Safety and Health Fact Sheets can also be downloaded. A partial list of Fact Sheets includes the following:
• Fumes and Gases
• Radiation
• Noise
• Electrical Hazards
• Fire and Explosion Prevention
• Burn Protection
• Mechanical Hazards
• Tripping and Falling
• Falling Objects
• Confined Spaces
• Contact Lens Wear
• Ergonomics in the Welding Environment
• Graphic Symbols for Precautionary Labels
• Pacemakers and Welding
• Electric and Magnetic Fields (EMF)
• Lockout/Tagout
• California Proposition 65
• Fluxes for Arc Welding and Brazing: Safe Handling and Use
• Metal Fume Fever
• Arc Viewing Distance
• Oxyfuel Safety: Check Valves and Flashback Arrestors
• Grounding of Portable and Vehicle Mounted Welding Generators
• Cylinders: Safe Storage, Handling and Use
Safety information is also available from manufacturers of welding equipment and consumables. Warning labels on machines and consumable packaging should be read and followed. Material safety data sheets (MSDSs) should also be read and followed.
Source: AISC Design Guide 21

## Slide 44: Weld Inspection
Primarily addressed in AWS D1.1 Section 6
Unless specified in contract documents, visual inspection is only method required
Nondestructive testing (NDT) requirements are to be stated in bid documents: including types of welds to be examined, extent of examination, and method(s) of testing
All welders, welding operators, and tack welders who perform work governed by the code must be qualified as prescribed in the code
Notes: Inspection issues are primarily addressed in AWS D1.1 Section 6.
Unless nondestructive testing is specified in the contract documents, the only inspection required by AWS D1.1 is visual inspection, performed by the contractor’s inspector (except for a couple of minor exceptions). Unless specified, there will be no nondestructive testing, no independent verification inspection—only the code-mandated visual inspection typically performed by an employee of the contractor. The engineer should consider what inspection and nondestructive testing, if any, is required beyond visual inspection and state the appropriate requirements in the contract documents. Subsequent revision of contract requirements after the fact is addressed in AWS D1.1 Provision 6.6.5 as follows: “If NDT other than visual inspection is not specified in the original contract agreement but is subsequently requested by the Owner,…the owner shall be responsible for all the associated costs including handling, surface preparation, nondestructive testing, and repair of the discontinuities at rates mutually agreeable between the owner and the contractor.” Note, however, that AWS D1.1 Provision 6.6.5 continues that “If such testing should disclose an attempt to defraud or gross nonconformance to this code, repair work shall be done at the contractor’s expense.”
Nondestructive testing (NDT) requirements are to be stated in the bid documents, including the types of welds to be examined, the extent of examination, and the method or methods of testing. The engineer must determine whether verification inspection is required. Verification inspection is independent of the contractor, and the results of it are reported to the engineer. This provision permits the engineer to waive verification inspection, perform all inspection functions with the verification inspector, or use both fabrication/ erection and verification inspection (AWS D1.1 Provision 6.1). The code provides three bases for qualifying inspectors and then states that, “If the engineer elects to specify the bases of inspector qualification, then it shall be so stated in contract documents.” The engineer is authorized to verify the qualification of inspectors.
“Any special inspection requirements” are required to be noted on the drawings or in the specifications. When specified by the engineer, ultrasonic inspection (UT) raises a number of opportunities for the engineer’s involvement. For example, AWS D1.1 Annex “K” contains alternate techniques for UT of welds, but the use of the annex procedures is subject to approval by the engineer. Annex “K” allows for inspection of welds beyond the conditions stated in AWS D1.1 Section 6, Part “F,” and includes variations such as other weld geometries, transducer sizes, frequencies, couplants, painted surfaces, and testing techniques, but such variations must be approved of in the contract documents (AWS D1.1 Provision 6.20.2).
All welders, welding operators, and tack welders who perform work governed by the code must be qualified by test as prescribed in the code. In most situations, contractors will have previously qualified their workforce in other projects, and the code extends to the engineer the option of approving the use of previous personnel qualification tests, eliminating the need for retesting (AWS D1.1 Provision 4.1.2.1).
Inspector Qualification
The engineer’s involvement in approving the qualifications of personnel includes inspectors (AWS D1.1 Provision 6.1.4.5).
Source: AISC Design Guide 21

## Slide 45: Weld Inspection
Visual Inspection
Inspection tasks that should take place after welding include
the following:
1. Inspect final weld appearance (porosity, undercut, cracks, etc.).
2. Inspect final weld size.
3. Inspect weld length.
4. Confirm the presence of all required welds.
5. Verify the absence of unauthorized welds.
6. Check for excessive distortion.
Notes: Welds are inspected to ensure that they comply with the requirements of a given specification. Weld inspection fits into two broad categories: destructive and nondestructive. Destructive testing typically involves machining test specimens out of a weldment, applying a force, and measuring the response of the test specimen to the force. The weldment is no longer useful for the intended service. Destructive testing is applied to welding procedure qualification test plates and may include tensile testing, Charpy impact testing, and bend tests.
Visual inspection is the most powerful tool that can be employed to ensure weld quality. The more technologically sophisticated nondestructive processes, such as ultrasonic or radiographic inspection, can only determine whether or not the specified quality is present once welding is complete. In contrast, since effective visual inspection examines each step of the welding process well before the weld is completed, it can be used to mitigate or avoid situations that could cause weld quality problems. Visual inspection (VT) is the only inspection method that, in and of itself, can actually improve the quality of a given weld. For example, visual inspection of the weld joint preparation and the adequacy of the root opening dimension can ensure that conditions conducive to obtaining good fusion are present before welding begins, minimizing the probability of incomplete fusion in the completed weld.
Everyone involved in a welding project, including the welders, inspectors, foremen, etc., can and should participate in in-process visual inspection. Minor discontinuities can be detected and corrected during the fabrication process, precluding the need for more expensive and complicated repair after the fabrication is complete. In order to be effective, visual inspection must take place prior to, during, and after welding. VT requires good eyesight and good lighting.

## Slide 46: Weld Inspection
Nondestructive Testing
Penetrant testing – liquid dye detects surface-breaking discontinuities by absorbing penetrant into the defect
Notes: Nondestructive testing (NDT) is an important element of many quality programs. It cannot, however, replace in process visual inspection. Before NDT is performed, AWS D1.1 requires that the welds first meet visual acceptance criteria (AWS D1.1, Provision 6.11). Because of the diversity of projects that can be governed by AWS D1.1, it is impossible for a single document to specify appropriate inspection requirements, including the extent and type of NDT to be performed, acceptance criteria, and who is responsible for various inspection tasks.
AWS D1.1, therefore, relies on the engineer to specify such NDT requirements. With a few exceptions, when no NDT is specified only visual inspection will be required by AWS D1.1 and the AISC Specification. Therefore, it is critical that any NDT requirements be established in advance of fabrication, under the direction of the engineer. It is the engineer’s responsibility to determine whether verification inspection will be utilized or whether reliance upon fabricator/erector inspection will be sufficient. It is important that everybody on the project, including the various inspectors, welding supervisors, and the welders themselves, understand what is expected of them before construction begins.
There are a variety of NDT methods available to inspect welds, each with advantages and limitations. Discussed on the next few slides are the four methods most commonly used, along with visual inspection, to inspect structural steel welds.
Liquid penetrant testing, also known as dye penetrant testing, involves the application of a liquid which, by a capillary action, is drawn into a surface-breaking discontinuity, such as a crack or porosity. When the excess residual dye is carefully removed from the surface, a developer is applied to absorb the penetrant that is contained within the discontinuity. This results in a stain in the developer showing that a discontinuity is present.
Conceptually, PT is simple, but in application, it is frequently misapplied. The materials being inspected must be clean. Adequate time, typically around 15 minutes, must be allowed for the liquid to be carried by capillary action into the discontinuity. Excessive liquid must then be carefully removed. Failure to remove dye from the surface will cause
irrelevant indications. If the surface is flushed with cleaner, however, the dye can be washed from the cavity. Therefore, only wiping of the surface is permitted. Finally, if the developer is applied but an insufficient length of time elapses before inspection, the dye may not stain the developer.
With respect to weld testing, a common mistake is to apply the dye when the part is still hot. This can cause the dye to boil or burn, and either not penetrate the discontinuity, or “dry out,” yielding unreliable results. Dye penetrant testing is effective for detecting only surface-breaking discontinuities. It has no ability to reveal subsurface discontinuities, but it is highly effective in accenting discontinuities that may be too small to detect with visual inspection alone. PT can be messy and slow. Because of these disadvantages and the fact that penetrant inspection is limited to surface-breaking discontinuities, and since these discontinuities can also be observed with magnetic particle inspection, PT is not commonly used for steel applications. PT is most often used to inspect nonmagnetic materials such as aluminum or austenitic stainless steel.
Source: AISC Design Guide 21

## Slide 47: Weld Inspection
Nondestructive Testing
Magnetic Particle Inspection (MT) – magnetic flux used and different patterns of magnetic powders form where discontinuities exist
Notes: Magnetic particle inspection utilizes the change in magnetic flux that occurs when a magnetic field is present in the vicinity of a discontinuity. When magnetic powders are dusted on the part, the change in magnetic flux density will create a different pattern where a discontinuity exists. The process is effective in locating discontinuities that are on the surface and slightly subsurface. For steel structures, magnetic particle inspection is generally preferred over penetrant inspection, as it is faster, less messy, can be performed on hot weldments, and can detect some subsurface discontinuities. Magnetic particle inspection can reveal cracks, incomplete fusion, slag inclusions, and porosity, Current is either directly passed through the material, or a magnetic field is induced through a coil on a yoke. With the first method, electrical current is passed through two prods that are placed in contact with the surface. When the prods are initially placed on the material, no current is applied.
After intimate contact is ensured, current is passed through. Small arcs may occur between the prods and the base material, resulting in an arc strike, which may create a localized brittle zone. It is important that the prods be kept in good shape and that intimate contact with the work is maintained before the current is passed through the prods. Depending on the geometry of the part, two people are often needed to perform MT with the prod method—one to hold the prods (one in each hand) and the other to apply the metallic powder.
The second method of magnetic field generation is through induction. In what is known as the yoke method, an electrical coil is wrapped around a core, often with articulated ends. Electrical current is passed through the coil, creating a magnetic field in the core. When the ends of the yoke are placed in contact with the part being inspected, the magnetic field is induced into the part. Since current is not passed into the part, the potential for arc strikes is eliminated. Along with this significant advantage comes a disadvantage; the yoke method is not as sensitive to subsurface discontinuities as the prod method. However, since MT is typically used to detect surface-breaking discontinuities, and since the prod method can create undesirable arc strikes, the yoke method is the most popular.
Cracks are most easily detected when they lie perpendicular to the magnetic field. With the prod method, the magnetic field is generated perpendicular to the direction of current flow. For the yoke method, the opposite applies. Magnetic particle inspection is most effective when the region is inspected twice: once with the field located parallel to the weld axis and once with the field perpendicular to the weld axis. While magnetic particle inspection can detect some subsurface discontinuities, it is best viewed as an enhancer of visual inspection. MT is not routinely used as an NDT method for inspecting structural steel welds, but is often used when visual inspection or other forms of NDT detect defects that need to be repaired. For example, MT may be used to ascertain the extent of cracking; part of the crack may be obvious, but the full extent of cracking may not be so apparent. MT can be used to determine the length or the depth of the crack. After the repairs are completed, MT is often used to ensure the quality of the repaired weld, particularly when the weld involved is a PJP groove weld or fillet weld.
MT is highly sensitive, and powder routinely collects along defect-free weld toes, for example, yielding irrelevant indications. Yet this is also the location where lamellar tearing or heat-affected zone cracking may occur. When disputes over the significance of an indication arise, careful selective grinding can eliminate the naturally occurring geometric change and the part can be reinspected. but all must be surface-breaking (or very near the surface). Permanent magnets can be used for MT to induce the magnetic field, but it is more common to create electromagnetic fields with electrical power.
Source: AISC Design Guide 21

## Slide 48: Weld Inspection
Nondestructive Testing
Radiographic Inspection (RT) – X / gamma rays expose radiographic film on opposite side of weld
Notes: Radiographic inspection uses X rays or gamma rays that are passed through the weld and expose a radiographic film on the opposite side of the joint. X rays are produced by high-voltage generators, while gamma rays are produced by atomic disintegration of radioactive isotopes. Whenever radiography is used, precautions must be taken to protect workers from exposure to excessive radiation.
Safety measures dictated by the Occupational Safety and Health Administration (OSHA), the National Electrical Manufacturer’s Association (NEMA), the Nuclear Regulatory Commission (NRC), the American Society of Nondestructive Testing (ASNT), and other agencies should be carefully followed when radiographic inspection is conducted.
Radiographic testing relies on the ability of the material to allow some of the radiation to pass through, while absorbing part of this energy within the material. Different materials have different absorption rates. Thin materials will absorb less radiation than thick materials. The higher the density of the material, the greater is the absorption rate. As different levels of radiation are passed through the materials, portions of the film are exposed to a greater or lesser degree than the rest.
Since the source of radiation must be on one side of the part, and the film on the other, access to both sides of the joint is required for RT. When the film is developed, the resulting radiograph will bear the image of the plan view of the part, including its internal structure. A radiograph is actually a film negative in which the darkest regions are those that were most exposed, since the material being inspected absorbed the least amount of radiation. Thin parts will be darkest on the radiograph. Porosity will be revealed as small, dark, round circles. Slag is also generally dark, and may look similar to porosity, but will be irregular in its shape. Cracks that lie parallel to the source of radiation appear as dark lines. Incomplete fusion and underfill will show up as darker areas. Weld reinforcement will result in a lighter region.
Radiographic testing is most effective for detecting volumetric discontinuities such as slag and porosity. When cracks are oriented perpendicular to the direction of the radiation source (e.g., parallel to the film), they may be missed with the RT method. Cracks that are parallel to the radiation path are the most detectable, although tight cracks have gone undetected by RT at times.
Radiographic testing has the advantage of generating a permanent record for future reference. With a “picture” to look at, many people are more confident that the interpretation of weld quality is meaningful. However, reading a radiograph and interpreting the results requires stringent training, so the effectiveness of radiographic inspection depends to a great degree on the skill of the technician.
Radiographic testing is ideally suited for inspection of complete joint penetration (CJP) groove welds in butt joints.
It is not suitable for inspection of partial joint penetration (PJP) groove welds or fillet welds. When applied to T- and
corner joints, the geometric constraints of the applications make RT inspection difficult, and interpretation of the results is highly debatable.
Source: AISC Design Guide 21

## Slide 49: Weld Inspection
Nondestructive Testing
Ultrasonic Testing (UT) – transmits high frequency sound waves that detects defects in the return wave
Notes: Ultrasonic inspection relies on the transmission of high frequency sound waves through materials. Solid, discontinuity-free materials will transmit the sound throughout a part uninterrupted. A receiver “hears” the sound reflected off of the back surface of the part being inspected. If a discontinuity is contained between the transmitter and the backside of the part, an intermediate signal will be sent to the receiver, indicating the presence of this discontinuity. The pulses are read on a display screen. The magnitude of the signal received from the discontinuity is proportional to the amount of reflected sound. This is indirectly related to the size, type, and orientation of the reflecting surface. The relationship of the signal with respect to the back wall will indicate its location. Ultrasonic inspection is sensitive enough to detect small discontinuities that are not relevant to the performance of the weld.
UT is most sensitive to planar discontinuities, such as cracks, laminations, and planes of incomplete fusion that
lie perpendicular to the sound path. Under some conditions, uniformly cylindrical or spherical discontinuities can be
overlooked with UT. Ultrasonic inspection is ideal for inspection of CJP groove welds in butt, corner, and T-joints. While UT inspection of PJP groove welds is possible, interpretation of the results can be difficult. Except with very specialized techniques, UT is not suitable for inspecting fillet welds.
A common problem in UT inspection involves T- and corner joints. When CJP groove welds are made from one side and with steel backing attached, the interpretation of results near the root is problematic at best. It is difficult to clearly distinguish between the naturally occurring regions where the backing contacts the adjacent vertical T- or corner joint member and an unacceptable incomplete fusion. There is always a signal generated from this area. Of course, this is the situation encountered when steel backing is left in place on a beam-to-column moment connection. To minimize this problem, the steel backing can be removed, offering two advantages: First, the influence of the backing is obviously eliminated; and secondly, in the process of backing removal, the joint can be backgouged and the root visually inspected prior to the application of the back weld and the reinforcing fillet weld. It is also important to note that when a bottom beamto-column connection is inspected, it is impossible for the operator to scan across the entire width of the beam flange because of the presence of the beam web. This leaves a region in the center of the weld that cannot be UT inspected.
Unfortunately, this is also the region where it is most difficult for the welder to deposit sound weld metal, and it has been identified as the location of many weld defects. When the beam is joined to a wide flange column, this is also the most severely loaded portion of the weld. Backing removal and subsequent backgouging operations help to overcome this UT limitation since they enable visual verification of weld soundness.
Source: AISC Design Guide 21

## Slide 50: 3 - Constructability considerations
Erection & Safety
Bolt Inspection
Weld Safety & Inspection
Base Plate Connections
Splices
Tolerances
Best Practices for Connections

## Slide 51: Base plate Connections
Connection of steel columns to concrete foundation below (typically concrete pier or spread footing)
Notes: Grouting shall be the responsibility of the owner’s designated representative for construction. Leveling plates and loose base and bearing plates shall be promptly grouted after they are set and checked for line and grade. Columns with attached base plates, beams with attached bearing plates and other similar members with attached bearing devices that are temporarily supported on leveling nuts and washers, shims or other similar leveling devices, shall be promptly grouted after the structural steel frame or portion thereof has been plumbed.
Commentary Source: AISC Code of Standard Practice:
Figure Source: Design Guide 1 – Base Plate and Anchor Rod Design, Fig. 1.1 – Column base connection components

## Slide 52
STRUCTURE OF THE EVERYDAY: Structural Steel Connections, AISC Teaching Aid by David Thaddeus (UNC Charlotte)
Base Plate Connection
Notes: This embedded video shows the very basics of a column base plate connection. Column base plates are typically installed below the floor level. Anchor bolts are typically placed prior to concrete casting of the foundations. Box outs are built around the column prior to casting the floor. This diamond box out around the column must then be filled in with concrete.

## Slide 53: Base plate Connections
Base plates and anchor rods transfer gravity and lateral loads from steel superstructure to the concrete foundation
Often the last structural steel items to be designed, but the first items required for erection on the jobsite
Accurate placement of anchor rods is crucial to safe and efficient erection and accurate plumbing of the building.

## Slide 54: Base plate Connections
OSHA Requirements
Safety Standards for Steel Erection require a minimum of four anchor rods in column-base-plate connections.
Base plate connections must have sufficient moment strength to resist a minimum eccentric gravity load of 300 pounds located 18 in. from the extreme outer face of the column in each direction.
Four anchors
Notes: The regulations of the Occupational Safety and Health Administration (OSHA) Safety Standards for Steel Erection (OSHA, 2001) require a minimum of four anchor rods in column-base-plate connections. (Per Section 1926.755(a)(1) of Standard 29 CFR)
The OSHA criteria can be met with even the smallest of anchor rods on a 4-in. by 4-in. pattern.

## Slide 55: Base plate Connections
OSHA Requirements
Why 18” and 300 lb?
Represents the weight of an erector hanging from a column
Failure of anchors may occur if not designed for moments / uplift during erection

## Slide 56: Base plate Connections
Anchor rods typically have a heavy hex nut or a headed or hooked end which is cast in place during concrete placement
Anchor rods for gravity columns are often not required for the permanent structure and need only be sized to provide for column stability during erection
Use 3/4-in. diameter ASTM F1554 Grade 36 rod material whenever possible for adequate strength and ductility
Hooks have a lower capacity

## Slide 57
Columns are typically shop-welded to the base plates with anchor and grout holes.
Grout holes (for placing grout)
Anchor rod holes

## Slide 58: Base plate connections
When laying out anchor rods adjacent to walls/other obstructions, ensure erectors have necessary access to tighten anchor rods
Anchor rod layouts must be coordinated with the concrete rebar to ensure rods can be installed in the proper location and alignment
Notes: Proper alignment of anchor rods is especially critical in concrete piers and walls where there is less room for adjustment in the field.

## Slide 59: Base plate connections
Layout (and after-placement surveying) of all anchor rods should be done by an experienced construction surveyor
Templates can be used to ensure proper anchor rod layout

## Slide 60: Base plate connections
The most common field problem is anchor rod placement: matching the holes in the base plate with the anchors located in the concrete
OSHA requires any modification of anchor rods to be approved by the Engineer of Record (EOR)
Larger holes in base plate help to accommodate setting tolerances

## Slide 61: 3 - Constructability considerations
Erection & Safety
Bolt Inspection
Weld Safety & Inspection
Base Plate Connections
Splices
Tolerances
Best Practices for Connections

## Slide 62: Column splices
Splices allow columns to be fabricated and transported in shorter lengths (typically 50 ft lengths or less)

## Slide 63: Column splices
Erection hole for lifting column with crane
Field-bolted connections typically preferred over field-welded connections

## Slide 64: Column Splices

## Slide 65
STRUCTURE OF THE EVERYDAY: Structural Steel Connections, AISC Teaching Aid by David Thaddeus (UNC Charlotte)
Field-bolted Column Splice
Notes: This is an embedded video showing a field-bolted column splice, which is far more common than the field-welded option.

## Slide 66
STRUCTURE OF THE EVERYDAY: Structural Steel Connections, AISC Teaching Aid by David Thaddeus (UNC Charlotte)
Field-Welded Column Splice
Notes: This is an embedded video showing a field-welded column splice.

## Slide 67: Column splices
Column splices typically 4-5 ft above finished floor
Splicing typically occurs at every other level.
Like base plates, must be designed for 300 lb. of load acting 18” from column
Notes: Column Splice Locations: Since connectors are required to tie off when the fall distance exceeds 30 feet, placing column splices every three floors is a bad choice for the purposes of erection. The erector will erect two floors, deck the second level, and then erect and deck the third level before starting the process again. It would be better for the designer to place column splices either every 2 floors or, in some cases, every 4 floors so as to optimize the erection process.
Except where constructability does not permit, perimeter columns must extend a minimum of 48” above the finished floor so as to allow the attachment of safety cables.
OSHA 1926 Subpart R 1926.756(e)(1): “The perimeter columns extend a minimum of 48 in. (122 cm) above the finished floor to permit installation of perimeter safety cables prior to erection of the next tier, except where constructability does not allow.”
1926.756 (e)(2) states: “The perimeter columns have holes or other devices in or attached to perimeter columns at 42 to 45 in. (107- 114 cm) above the finished floor and the midpoint between the finished floor and the top cable to permit installation of perimeter safety cables required by § 1926.760(a)(2), except where constructability does not allow.”
The 4-ft (1.2-m) column extension limit is sometimes not enough since it can cause an interference between the splice plates and the holes for the safety cable. For constructability reasons, it is recommended that the column splice be conservatively located at 5 ft (1.5 m) above the top of the beam

## Slide 68: Column Splices

## Slide 69: Beam Splices
Beam splices typically only used if it will significantly improve constructability and/or relieve transportation issues
  i.e. – used often in bridge girders, as the girders would be too long to transport at their full length
Connection is designed in such a way that it behaves as if it were one continuous beam instead of two beams simply connected together

## Slide 70: Beam Splices
Flange plates transfer moment, web plate transfers shear
Field-bolted connections typically preferred over field-welded connections

## Slide 71: Beam Splices
Field-bolted Beam Splices
STRUCTURE OF THE EVERYDAY: Structural Steel Connections, AISC Teaching Aid by David Thaddeus (UNC Charlotte)
Notes: This is an embedded video showing a field-bolted beam splice.

## Slide 72: 3 - Constructability considerations
Erection & Safety
Bolt Inspection
Weld Safety & Inspection
Base Plate Connections
Splices
Tolerances
Best Practices for Connections

## Slide 73: Tolerances
Beam Length Tolerance
Provide setbacks where possible for ease of erection
    Minimum clearance of ½” should be provided when connecting members

## Slide 74: Tolerances
 | Length | Max. Variation
Beams | L ≤ 30 ft | 1/16”
 | L 30 ft | 
 | Length | Max. Variation
Beams | L ≤ 30 ft | 
Beam Length Tolerance
Per Code of Standard Practice, for members that have both ends finished for contact bearing:
Notes: For members that have both ends finished (see Section 6.2.2) for contact bearing, the variation in the overall length shall be equal to or less than 1 /32 in. (1 mm). For other members that frame to other structural steel elements, the variation in the detailed length shall be as follows: For members that are equal to or less than 30 ft (9 000 mm) in length, the variation shall be equal to or less than 1 /16 in. (2 mm). For members that are greater than 30 ft (9 000 mm) in length, the variation shall be equal to or less than 1 /8 in. (3 mm).
Neither the ±1∕16-in. tolerance, where applicable, on overall length of members framed to other steel parts nor the 1∕16-in. clearance on size of standard holes should be construed as implying that the tolerance of ±1∕16 in. also applies either to the maximum tolerance on hole location within a pattern of holes or to the position of intermediate connections.
Source: AISC Code of Standard Practice (COSP)

## Slide 75: Tolerances
Beam Length Tolerance
Beams with plate or angle connections to the web may have beam lengths that vary by ¼” at either end (i.e. ½” shorter or longer than detailed) – this is a typical beam cutting tolerance.
Good practice to use detailed edge distance minus ¼” for design calculations, to be conservative.
Notes: The steel detailer should endeavor to allow the shop as much variation in length as possible, up to the full mill tolerance. If full mill tolerance or something approaching it can be allowed at each end, the shop does not have to divide the mill overrun or underrun equally at each end. For many shops, the +/- ¼” tolerance is a standard amount and the steel detailer does not have to show it on the shop drawings. However, tolerances other than standard must always be shown. The detail should meet the standards of the employing fabricator.
Source: AISC Detailing for Steel Construction

## Slide 76: Tolerances
Beam Length Tolerance
Example of a shop drawing
Bolt-to-Bolt Longitudinal Distance Held
Edge may vary +/- ¼”
-3/4
-3/4
Setback
1/4
1/4
Cutting tolerance
Longitudinal distance between open holes would need to be held to match supporting member details – this distance can not vary.
Notes: The minus dimensions (-3/4) shown outside are the setback dimensions, the distances from the centerline of the supporting columns to the end of the beam.
The overall length of the beam is used to determine the setbacks by subtracting its length from the distance center-to-center of support columns.
The 18’4 ½” length is the ordered length, probably determined long before the detail is made. Had it been ordered slightly longer or shorter, it still would be used as ordered, provided that erection clearances are adequate, end or edge distances meet minimum AISC Specification requirements, and the design bearing strength is adequate.
The plus-and-minus figures (+/- ¼”) shown at the ends of the web view tell the shop that the beam length can vary up to a total of ½” shorter or longer than detailed. Therefore, the beam would be usable without trimming, provided its length is between 18’4” and 18’5”. The shop would adjust the edge distance, shown as 2 ¼” and the length of clearance cuts, shown as 4 ¼” to suit. The longitudinal distance between bolts (18’0”) must be held.
Source: AISC Detailing for Steel Construction

## Slide 77: Tolerances
Bolt Hole Tolerance
Maximum dimensions of standard, oversized, short- slotted and long-slotted holes are given in AISC Specification Table J3.3.
The RCSC Specification (in the footnote of Table 3.1) allows a 1∕32-in. tolerance on these maximum hole sizes.

## Slide 78: Tolerances
During the course of erection, it occasionally becomes necessary to ream holes so fasteners can be installed without damage to the threads, resulting in a hole that is larger than normal or elongated.
Reamed holes must meet the provisions for minimum spacing and minimum edge distance in AISC Specification Sections J3.3 and J3.4.
If major misalignment occurs, the error must be corrected by the responsible entity (report to owner, fabricator, engineer, etc.)
Notes: During the course of erection, it occasionally becomes necessary to ream holes so fasteners can be installed without damage to the threads, resulting in a hole that is larger than normal or elongated. The hole types recognized by the AISC and RCSC Specifications are standard, oversized, short-slotted and long-slotted, with nominal dimensions as given in the AISC Specification Table J3.3. The AISC Code of Standard Practice Section 7.14 Commentary states: "The term ‘moderate’ refers to the amount of reaming, grinding, welding or cutting that must be done on the project as a whole, not the amount that is required at an individual location. It is not intended to address limitations on the amount of material that is removed by reaming at an individual bolt hole, for example, which is limited by the bolt-hole size and tolerance requirements in the AISC and RCSC Specifications." Note that reamed holes must meet the provisions for minimum spacing and minimum edge distance in AISC Specification Sections J3.3 and J3.4, respectively.
When more major misalignments occur, it is indicated in the AISC Code of Standard Practice Section 7.14 that they are “promptly reported to the [owner] and the fabricator by the erector, to enable the responsible entity to either correct the error or approve the most efficient and economical method of correction to be used by others.”
Source: AISC Steel Solutions 2.5 – Correction of Fabrication Errors

## Slide 79: ToleranceS
Field Adjustment
Allow for field adjustment in only one direction at bolted connections.
If slotted holes are needed at a bolted connection for field adjustment, the adjustment should be in only one direction.

## Slide 80: Tolerances
Base Plate Holes
Extra-oversize holes recommended in base plates to accommodate dislocation possibilities in the anchor rod.
Vertical variation in location : equal to or less than ½”
Horizontal variation in location :
Anchor Rod Diameter, in. | Horizontal Variation, in.
and | 
1, 1 ¼, 1 ½ | 
1 ¾, 2, 2 ½ | 
Anchor Rod Diameter, in. | Horizontal Variation, in.
1, 1 ¼, 1 ½ | 
1 ¾, 2, 2 ½ | 
Notes: From Code of Standard Practice (COSP) Section 7.5.1

## Slide 81: 3 - Constructability considerations
Erection & Safety
Bolt Inspection
Weld Safety & Inspection
Base Plate Connections
Splices
Tolerances
Best Practices for Connections

## Slide 82: Best practices for Bolted connections
Limit the number of bolt diameters to one size (a maximum of three sizes if necessary)
Avoid different grade bolts with the same diameter
When possible, use 1 1/8” diameter bolts or smaller
When permitted by the engineer of record (EOR): use oversized holes in beam moment and brace connections
Notes: Limit the number of bolt diameters to one size: This reduces field errors as well as fabrication errors with drill lines that have manually changed spindles. Some fabricators/erectors keep at least a ¼” difference between bolt sizes to prevent uncertainty
Avoid different grade bolts: To avoid using a lower grade bolt accidentally. If ASTM A325 and A490 bolts of the same nominal diameter are mixed on a project, there exists the possibility that the A325 bolts might be installed where the A490 bolts were required. Therefore, when ASTM A325 and A490 bolts are used on the same project, quality assurance is simplified if different diameters are used for different grades.
Use 1 1/8” diam. bolts or smaller: The industry standard ¾-in., 7⁄8-in. and 1-in. bolt diameters provide adequate design strength for the vast majority of connections in steel structures. Accordingly, commonly available bolt installation equipment has been designed with a capacity to fully tension 1-in. diameter ASTM A490 bolts when required; larger bolts will usually require special equipment and/ or effort. Additionally, bolt diameters larger than 1 in. may require larger clearances, edge distances, and spacings than are standard. Therefore, bolt diameters larger than 1 in. should be avoided, when possible, to help prevent potential bolt tensioning difficulties.
Use oversized holes in beam moment and brace connections: At flange-plated moment connections or brace connections with slip-critical bolts, oversized bolt holes are often preferred over standard bolt holes. Although standard holes give a greater bolt capacity, oversized holes permit more erection tolerance and reduce field problems. Typically, oversized holes are used in the detail material and standard holes in the main member.
Source: “30 Good Rules for Connection Design” Carol Drucker, Modern Steel Construction, May 2004.
Source: SteelWise – The Nuts and Bolts of Nuts & Bolts” Larry Muir, Modern Steel Construction, May 2015.

## Slide 83: Best practices for Welded connections
Avoid overhead welding
Use full-penetration welds only when necessary
Minimize fillet weld size when possible to avoid multiple weld passes
Use fillet welds when possible
Notes: Avoid overhead welding: The preferred welding positions are flat and horizontal. Overhead welding is difficult, costly and generally yields lower quality welds. For single-pass SMAW fillet welds, it can take four times as long as welding in the flat or horizontal position. In the flat position, the base metal provides support for the molten pool of weld metal. Therefore, this position provides for the fastest deposition rate and the most economical weld. Welding in the horizontal position is similar, but slightly less efficient. Welding in the vertical or overhead position requires slower deposition rates to maintain the integrity of the molten pool against the effects of gravity.
Use full-penetration welds only when necessary: Full-penetration welds cost more than partial-penetration or fillet welds due to increased material preparation, testing requirements, weld-metal volume and material distortion. Use fillet welds (provided that the fabricator does not determine them excessively large) or partial penetration welds when joint strength is adequate for the applied load. Full-penetration welds at HSS members are difficult due to the need for backing bars
Because the volume of weld metal in a fillet weld is proportional to the square of the weld size, a 1/2-in. fillet weld uses four times as much weld metal as a 1/4-in. fillet weld of the same length. Because the cost of welding is essentially proportional to the volume of weld metal, the most economical fillet-welded detail will result when the least possible fillet weld size is used. Accordingly, it is common practice in welded joint design to select fitting and weld length to minimize fillet weld size, when possible. Additionally, smaller welds reduce the possibility of warping and distortion due to heat input.
Fillet welds generally require less weld metal than groove welds. Additionally, fillet welds do not generally require beveling and similar base metal preparation. As a result, fillet welds are generally more economical to make than groove welds. Thus, fillet welds are preferred.
Minimize fillet weld size: The number one cost in welding is that of the skilled labor required to make a weld. In general terms, labor will account for 75 to 95 percent of the cost of a weld made manually or semi-automatically. Energy costs, filler metals, and shielding materials make up the remaining 5 to 25 percent. For a given weld size, economical welding is typically achieved when welding procedures are used that deposit the required metal in the least amount of time. Quality and safety should never be compromised for the sake of productivity. It is not unusual, however, to make quality welds in a safe manner with procedures that are twice as productive as another otherwise acceptable alternative. In general terms, a welding procedure that deposits the required metal twice as fast will reduce the welding cost by 50 percent.
Most of the principles below are presented in terms of reduced weld metal volumes, assuming that as the required amount of welding goes down, so will the required time to make the weld. There are two caveats: First, presenting these concepts in such terms runs the risk of implying that the major cost of welding is filler metal when, in fact, with North American labor rates, labor is invariably the largest single cost factor in welding. Second, there are situations wherein a weld joint requiring a larger volume of weld metal can be completed more rapidly than one requiring less metal, because it may be possible to deposit the metal at a faster rate in a joint requiring more metal.
Use fillet welds when possible: Fillet welds generally require less weld metal than groove welds. Additionally, fillet welds do not generally require beveling and similar base metal preparation. As a result, fillet welds are generally more economical to make than groove welds. Thus, fillet welds are preferred.
The lowest cost weld will always be the one that is made only once. The cost of a weld repair is estimated to be 10 times greater than the initial welding cost. If a particular weld design or welding procedure is marginal in its ability to consistently achieve the required quality criteria, necessitating ongoing weld repairs, economy can surely be achieved by adopting practices to eliminate the rework.
Source: AISC Design Guide 21
Source: AISC Steel Solutions Center – Engineering FAQs, 8.1 Economical Suggestions